## Slide 1: RTM (Resin Transfer Moulding)

## Slide 2: Liquid Molding

## Slide 3: RTM (Resin Transfer Moulding)

## Slide 4: “Alphabet soup” of RTM-type processes
RTM
  A technology developed starting from polyurethane reactive injection
  Injection in a closed mold in presence of a reinforcement preform
  Typical fibre content 30%-50% by volume, P about 6-10 bar
  Sandwich panels with foam cores
VARTM (Vacuum assisted RTM)
  Vacuum is applied to reduce he void content. A slight pressure increase is also obtained.
  Vacuum in the range 700-900 mbar
  - higher cost of equipments and molds
RTM light
  One of the mold is made using a composite laminate
  Vacuum is used but lower positive pressures allowed in comparison with RTM

## Slide 5: RTM vs. VARTM
RTM
  Both molds are made of steel or aluminum and are ususally put in a press.
  In absence of vacuum the air is pushed out by the resin.
  The injection is usually in a single point or in aline at the mold edge.
VARTM
  Equipment similar to those adopted for RTM
  Vacuum is applied
  Metal tooling with seals for vacuum

## Slide 6: RTM
RTM
Flow visualization using a transparent mold

## Slide 7: RTM vs. RTM light
RTM
  Both molds are made of steel or aluminum and are ususally put in a press.
  In absence of vacuum the air is pushed out by the resin.
  The injection is usually in a single point or in aline at the mold edge.
RTM light:
  With one of the mold in GFRP (or CFRP) max positive pressure is 1 bar
  Vaccumm is applied at the cemter and injection occurs along the perimeter, using a proper feeding channel

## Slide 8: Vacuum assisted resin distribution or resin infusion (VARI)
A resin trap an perforated release films are tipically used
Schraubzwinge
Spannrahmen
Dichtung
gelochtes Blech
Rinne für überflüssiges Harz
Folie
Verstärkung mit Laminat
Trennschicht
festes Werkzeugunterteil
Vakuumbehälter für überflüssiges Harz
Ventil zur Vakuumpumpe

## Slide 9: “Alphabet soup” of RTM-type processes
SCRIMP (Seeman’s Composite Resin Infusion Molding Process)
  The resin is sucked into the dry fibres thanks to vacuum
  an open mold is used. Vacuum bagging is applied
  In SCRIMP process the first resin distribution media were patented

## Slide 10: Resin distribution media (or nets)
Different materials characterized by a high permeability to the resin can be used as resin distribution media.
High permeability is required under vacuum, i.e. under 1 bar pressure.
The resin distribution medium acts also as breather when vacuum is applied
The use of a resin distribution medium or of a resin distribution net promote an in-plane flow in this high permeability material while the impregnation of the reinforcements is achieved by an out-of-plane (through-thickness) flow

## Slide 11: Resin distribution media or resin distribution nets (external)
Plastic wires are weaved so that the resin can flow in the same way in the two directions

## Slide 12: Resin distribution nets (external)

## Slide 13: Resin distribution nets (internal, acting as cores)
Plastic base net by Colbond (Enka – Spacer 7008)
Lantor Soric® (Lantor Composites)

## Slide 14: Internal (core) distribution media

## Slide 15: Resin distribution nets (internal) and lay up
Lantor Soric® (Lantor Composites)

## Slide 16: Grooved cores

## Slide 17: Resin infusion through a grooved core

## Slide 18: Liquid moulding in wind blade skins
PVC and balsa with distinctive groovings to enable the DIAB method of core infusion for the fabrication of 83 m wind blade. Each blade skin was produced in a female mould using a combination of VARTM (vacuum assisted resin transfer moulding), pre-preg and hand lamination

## Slide 19: Resin infusion of a sail boat hull

## Slide 20: Resin infusion of a sail boat hull: rinforcement at the mast base

## Slide 21: Resin infusion for a boat hull: deck

## Slide 22: Resin infusion of a boat hull: deck

## Slide 23: “Alphabet soup” of RTM-type processes (II)
RFI (Resin Film Infusion)
  A film of resin (high viscosity, poor or no tack) is stacked together with a dry reinforcement in a typical tool used for autoclave lamination
  Vacuum bagging and auxiliary materials formerly described are used
  Impregna tion and cure occurs in an autoclave
  Impregnation occurs when the viscosity decreases to the minimum befor gelation
  Transversal flow is limited to ply thickness distance

## Slide 24: “Alphabet soup” of RTM-type processes (II)
RFI (Resin Film Infusion)

## Slide 25: “Alphabet soup” of RTM-type processes
  CAPRI (Controlled Atmospheric Pressure Resin Infusion) was patented by Boeing
  it reduces thickness variation and results in fiber volumes and mechanical properties equivalent preprepreg/autoclave materials.
  First it uses vacuum debulking cycles on the dry preform to reduce compressed thickness prior to infusion.
  During infusion, the resin supply is held at partial vacuum, which assists in degassing the bulk resin but also reduces the pressure differential driving resin into the preform.
  Curing in autoclave or out of autoclave

## Slide 26: “Alphabet soup” of RTM-type processes
Rocco.Rametta@avioaero.com

## Slide 27: “Alphabet soup” of RTM-type processes
  VAP (Vacuum Assisted Process) was patented by EADS
  it is used in parts like the A380 Aft Pressure bulkhead and the massive A400 Cargo Door.
  VAP features a gas permeable membrane placed over the infused layup, which helps to evacuate trapped air and volatiles in the infused layup prior to cure.
  By letting gases through the membrane (but not the resin) VAP is said to achieve lower voids and higher, more controlled fiber volume for better laminate quality

## Slide 28: “Alphabet soup” of RTM-type processes
  RTI (Resin Transfer Infusion) is a Bombardier patented process used to produce the wing skins of its Cseries (now Airbus 220) aircraft using dry carbon fiber non-crimp fabric (NCF)
  The NCF has a binder, which is used in preforming on a male tool, followed by infusion in a female tool.
  The tool is preheated, the part is bagged and the resin (Cytec’s Cycom 890, for resin transfer molding) is injected with vacuum pressure only.
  However, the mold is located in an unpressurized autoclave during the infusion step. After the preform is fully infused, the autoclave is pressurized and heated to perform cure.
  This makes it easier to achieve high laminate quality because positive cure pressure (>14 psi) helps prevent void formation from entrapped air and volatiles. It has the drawback that a suitable size autoclave is still requited.
  Stringers are co-cured with the upper and lower wing skins

## Slide 29: RTM processes and toughned epoxy resins
Toughened epoxy resins contains thermoplastic chain segments among the oligomers used in the formulation. These are functionalized (epoxy or amine terminated) to react with the other monomers.
These compounds are responsible of a signifcant increase of the resin viscosity, too high for RTM (A in figure)
Soluble powders or fibers or coatings on fibers (Fig. 7) made of the toughening agents are adoptedinjection is performed with a low viscosity resin toughening occurs after dissolution of the thermoplastic powder or fiber or coating. Each of these act as binder in preforming
Epoxy resin viscosity during heating at constant rate:
A: Too viscous , B: too fast kinetic,
C: Viscosity profile needed for RTM

## Slide 30: toughned epoxy resins: Priform process
Temperature profile for Priform process:
  Toughening fibre dissolution occurs after mold filling
  Phase separation is the mechanism where thermoplastic domains are formed during curing, leading to a toughened crosslinked polymer.

## Slide 31: Benefits of RTM
Low capital investment (low pressures 6-8 bar)
Good surface quality
Tooling flexibility
Large, complex shapes
Ribs, cores and inserts
Parts integration
Range of available resin systems (all resins with viscosity lower than 0.8 Pa s)
Range of reinforcements (all fibers)
Controllable fiber volume fraction

## Slide 32: A “good” RTM resin
(0.2 Pa s)

## Slide 33: Darcy experiments on flow in porous media
V=Q/A= -(K/h) DP/L

## Slide 34: Darcy vs. Navier-Stokes
The average velocity is :
Assuming as Permeability coefficient K:
Darcy equation is obtained:
Integration of Navier-Stokes eqn for a tube in steady state provides the flow rate q, called Hagen-Poiseuille equation:
Dividing by the cross section area
In a porous medium with ni cylindrical pores of radius Ri the flow rate is:
i=1,N( number of cylindrical pores)
x
y
z
2R
q
b
h

## Slide 35: Darcy Equation
Local Reynolds number = rvD/h<1  laminar flow among pores
Darcy Equation
V = - [K]/h (ÑP-rg)
Vi= -1/h (Ki1¶P/¶x1+Ki2 ¶P/¶x2+Ki3¶P/¶x3)
where: [K] = permeability matrix
V = Q/A ed h = h(T,a)
Often g can be neglected and Kij = 0 per i¹j Kij¹0 per i=j
V1=-1/h K11¶P/¶x1 Vx=-1/h Kxx¶P/¶x
V2=-1/h K22 ¶P/¶x2 Vy=-1/h Kyy ¶P/¶y
V3=-1/h K33¶P/¶x3 Vz=-1/h Kzz¶P/¶z

## Slide 36: Continuity Equation
For an an incompressible flow field
  ¶Vx/¶x +¶Vy/¶y+ ¶Vz/¶z=0
Substituting Darcy equation:
¶/¶x(Kxx/h ¶P/¶x)+¶/¶y(Kyy/h ¶P/¶y)+¶/¶z(Kzz/h ¶P/¶z)=0
If K and h do not depend on x,y and z :
¶2P/¶x2+¶2P /¶y2+¶2P/¶z2=0
and in 1D  ¶2P/¶x2=0

## Slide 37: Integration of the continuity equation in 1D
Integrating ¶2P/¶x2=0  P=C1+C2x is obtained
B.C. : P=0 at x=xf (front position)
P=Pi at x=0 (Injection pressure Pi assumed constant at x=0)
P=Pi(1-x/xf)
the velocity (plug flow), given by Darcy eqn. decreases as xf increases
L
xf
x
xf
P
Pi
A steady state equation for an unsteady state problem?
The entrance length, where the velocity profile changes, is given by Li@ 0.05 D Re
but D @ 10-5 m and Re @10-110 Li is very small, of the order of 10-7 m

## Slide 38: Front position in 1D flow
Darcy equation in 1D is: Q/ATOT= Mean velocity Vm = - K/h dP/dx
IF V is the front velocity then Q= V ATOT (1- vf)
Assuming steady state flow at each time instant and being the flow incompressible, a plug flow occurs where velocity id given by V=dxf/dt
If injection ia achieved at constant pressure (DP=const.) then dxf/dt=- K/h (1- vf) DP/xf
Integrating for constant permeability and viscosity separating the variables : xdx=- K/h (1- vf) DPdt tra [0, xf] e [0, tf]
L
xf

## Slide 39: Front position in 1D flow
The calculation of the permeability of the reinforcement or of the distribution net can be made for the technology of resin infusion with a simple experimental set-up using the vacuum bag (usually transparent) and by recording the position of the front at different infusion times
The slope of the plot of resin front
position vs. t0.5 is:
L
xf

## Slide 40: Filling time 1D
Starting from the integration of dx/dt=- K/h DP/x it is possible to obtain the filling time, tr , i.e. the time needed to fill a mold length equal to L:
tr can be compared with tgel or to the induction time, obtained by rheological and/or calorimetric experiments

## Slide 41: Dimensionless Darcy equation
Dimensionless variable are: xf*=xf/(L/2) , t*=t/tgel e DP*= DP/(Pi /2)
L= flow length, Pi= injection pressure
Darcy eqn. dxf/dt=- K/h (1- vf) DP/xf becomes:
Where again Deborah is the ratio of two time scales:
Obviously DeD>1 is always required in order to completely fill a mold
(1- vf)

## Slide 42: Permeability measurement
The measurement of permeability can be also done by:
plotting flow rate vs. pressure drop for a one-dimensional flow experiment, and
measuring the slope of the linear portion of this graph.
This can be done according to Darcy’s experiment for out of plane permeability

## Slide 43: Effect of viscosity changes
As the resin polymerizes, the viscosity of the resin increases.
The gel time is the time at which there is a sharp rise in the viscosity of the resin as it starts to solidify into a cross-linked structure.
Gelation sets the time available for filling large parts.
The resin formulation may be changed to suit processing conditions.
Epoxy resin
Unsaturated
Polyester resin

## Slide 44: Fast curing resin for RTM
Epoxy and polyurethanes
High cure temperature materials
Automotive applications
Very low filling time required

## Slide 45: Permeability
Physical dimensions [K] = [h V L /P] = [P t L t-1 L P-1]= [L2]
Permeability depends on:
Porosity (f= 1- vf)
Type of reinforcement (glass, carbon etc.)
Shape and dimensions of pores
Sizing of fibres and type of resin (polyester, epoxy etc.)
In each direction K i proportional to f and to fibre radius Rf
Kii = Cii (R2f/4) [f3/(1-f)2 ]
Cii = Carman-Kozeny constant
Since it is not true that when porosity is zero then Kii =0, a limiting porosity value flim=(1-vfmax) at which Kii 0 is introduced
Kii = Cii (R2f/4) [(vfmax /vf-1)0.5]3/[vfmax /vf+1]
Notes: Pag. 226 liquid molding

## Slide 46: Anisotropic flow in RTM
Permeability for fluid flow in the plane is generally higher than its permeability for the fluid in the transverse or out-of-plane direction. (i.e. For a unidirectional woven Kzz<Kxx and Kzz<Kyy but also Kxx>Kyy; for a balanced woven fabric Kxx = Kyy)

## Slide 47: Effect of preform compressibility
The same reinforcement can be characterized by a different permeability depending on the fiber content, i.e. the thickness defined by mould and plug in RTM and the vacuum achieved in VARI

## Slide 48: Pressure drop in RTM (Darcy law)
Cross ply preform
The relationship between the pressure drop and the flow rate is linear and indicates the applicability of Darcy's law in both cases.
Knowing fluid viscosity, the length L and cross-sectional area A of the preform, its permeability can be calculated from the slope of the graph.
For the higher fiber volume fraction of 0.69, the slope is much less than the slope for the lower fiber volume fraction of 0.49. This shows that for higher volume fraction the preform permeability is much less, although both the preforms are made from the same uni-directional plies

## Slide 49: 1D flow in layers with different permeability
In reality, variations in permeability through the thickness of the part lead to racetracking and other non-plug flow profiles, so the simplified scheme is not perfectly accurate.

## Slide 50: Microscale flow
There are two scales of resistance to flow through preforms: resistance between the tows and resistance in the tows.
Even when a part appears completely filled, microvoids may remain if the resin does not wet the entire tow. This is more prone to happen at higher fiber volume fractions.
The pictures shows the tows as circles and the junctions as the areas around the tows. The flow entering can go past the tows without fully impregnating them.

## Slide 51: Micro-scale and meso-scale flow
The flow front comes around fiber tows and actually passes it. However, the fluid continues to impregnate the tow after the flow front has passed.
If the air was not evacuated at the beginning of the filling process, air is trapped in the tow and so a microvoid is formed at the center of the tow.

## Slide 52: Microscale flow
flow front
Fibre Bundles

## Slide 53: Microscale and macroscale flow
Resin
Resin
Permeability is different for the two type of matrix flow depending on porosity and tortuosity
Kmicro = Cmicro (R2f/4) [fmicro3/(1-fmicro)2 ]
Kmacro = Cmacro (R2bundle/4) [fmacro3/(1-fmacro)2 ]
Capillary forces are dominant on pressure forces very low DP Thermosetting resin: hand lay up
Pressure forces are dominant on capillary forces  high DPRTM
Typical of thermoplastic matrix impregnation
Notes: 2 Arten von POREN:
  Makroporen
  Mikroporen
Die Ersten lassen sich durch Massnahmen wie vorher betrachtet “einfach eliminieren”. Die zweiten erfordern die Betrachtung von Mikro und Makroflüssen
Die Fliessfront bewegt sich in zwei Ebenen:
  Microebene, d.h. im Faserbündel durch Kapillareffekte
  Macroebene, d.h. zwischen den Bündeln  Darcy
Die Erfahrung zeigt, dass es schwierig ist Luftblasen zu entfernen, wenn die Fliessfront fortgeschritten ist. 2 Möglichkeiten zur Steuerung der Entlüftung
  Vakuum
  Fliessfrontgeschwindigkeit (Bild)
Hohe Geschwindigkeit (Links): Bildung von Luftblasen in dem Faserbündel
Niedrige Geschwindigkeit (rechts): Bildung von Luftblase zwischen den Faserbündeln
Mögliche Masnahme: Druckerhöhung und gleichzeitig schliessen der Entlüftungsventile

## Slide 54: Micro e macro flow in resin transfer moulding (RTM)
Depending on the capillary number, Ca= hv/g: ViscosityXvelocity
Intrabundle or micro voids are observed. surface tension
Interbundle or meso-scale voids are observed
P Ermanni, Composite A, 2007
Usually the velocity, v, make the capillary number (>10-4) Only intrabundle voids are expected
Void content
10-4

## Slide 55: Micro e macro flow in resin transfer moulding (RTM)
Intrabundle or micro voids are observed.
Direction of flow
Mizutani, Adv.Comp.Mat. 2013

## Slide 56: Darcy flow in autoclave lamination
Step 1: room temperature very very high viscosity
Step 2: Temp. ibìncreases, viscosity decreases and the liquid escapes from the. Fiber bed is compacted
Step 3: the fiber beds start carrying load and its permeability reduces: the resin flow decreases
Step 4: if gelation is not occurred all the load is carried by spring (compacted fiber bed) the hydrostatic pressure in the liquid drops and void formation is likely to occur

## Slide 57: Process modeling: Vacuum bagging
Autoclave pressure reduces the breather thickness. A single layer of breather under 9 bar pressure with a thickness of 0.5 mm was adopted
At room temperature:
there is no flow
The top ply in the stack is kept under vacuum (between -700 and -980 mbar depending on the process)
tool
laminate
breather
vacuum
The resin flow in autoclave process can be sketched as a dashpot and a spring in parallel (a Maxwell-Voigt viscoelastic element).
The spring represents the stiffness of the reinforcement
The dashpot the viscous drag due to resin flow

## Slide 58: Darcy flow in autoclave lamination: heating and resin flow
During heating:
viscosity decreases
A pressure gradient is developed across the lay up
The resin flows through composite thickness filling the breather (in plane flow is neglected) under autoclave pressure
The upper resin layer still under vacuum
Resin filled breather
Unfilled breather
vacuum
xf
Resin front position

## Slide 59: Darcy flow in autoclave lamination: end of flow, pressure build up
When the resin touch the vacuum bag:
The flow ends
The pressure is distributed between those supported by the reinforcement, under compression strain, the hydrostatic pressure in the resin is constant
The resin pressure is always lower than autoclave pressure
autoclave pressure
bag/resin contact
vacuum

## Slide 60
tool
autoclave pressure
laminate
bleeder
autoclave pressure
autoclave pressure
vacuum
vacuum
vacuum
Room temperature
No flow.
Eventual lost of volatiles by diffusion
Heating: reinforcement compaction and flow.
Still possible volatile extraction
A three stage process and the viscoelastic model
Pressure is distributed between the spring (elastic reaction of fiber stack) and the dashpot (hydrostatic pressure in the resin)
vacuum bag in contact to resin
Flow end

## Slide 61
Other possible causes for flow end
The resin flow ends when:
  the bleeder is filled of resin(as formerly described) or
  the spring takes all the load or
  resin viscosity is very high and the dashpot becomes not deformable
Resin filled breather
Unfilled breather
vacuum
xf
Resin front position

## Slide 62: Modeling of pressure distribution
The total pressure, i.e. autoclave pressure is given by:
Paut=Psp+Pdp
Spring pressure (Psp) is given by a non linear
relationship:
Psp =A0exp(e/A1)-A0
A0 and A1 are assumed constant
e= vertical strain along X
Paut
Pdp
X
Psp
Stiff fiber stack
Vf about 45%
compliant fiber stack
Vf about 60%

## Slide 63: Darcy flow in autoclave lamination: Modeling of pressure distribution
The stress (pressure) supported by the dashpot was obtained assuming a Darcy flow across the reinforcement stack in 1D across the thickness
- Lateral flow is neglected
Pdp = (de/dt) ttoth(T, a)/Kf (tc -ettot)
The Viscosity h depends on Temperature and Degree of reaction
ttot= total thickness=stack (tc) +breather thickness
Kf is the permeability of the reinforcement and
depends on fiber content Vf
Therefore a first order differential eqn is obtained,
where e[a(T, t),h(a,T)] is the unknown:
Paut=Psp(e) +Pdp (e, de/dt)
Paut
Pdp
Psp
X

## Slide 64
Darcy flow in autoclave lamination: Stress in the fiber stack and resin pressure
Laminate thickness =12 mm
Compliant fiber stack
Bleeder thickness 0.5 mm
Heating rate =0.5 oC/min
Autoclave pressure 9 bar
High laminate thickness
Bleeder is filled but with a limited
strain of fiber stack
Autoclave pressure is almost equal
to equilibrium resin pressure
equilibrium hydrostatic resin pressure

## Slide 65: Hydrostatic resin pressure measurements
The stiff screen prevents deflection into the hole in contatct with the pressure transducer
Test with high and low flow resins in UD laminates
10 to 40 plies
Campbell, J. Adv. Mat. 1995

## Slide 66: Darcy flow in autoclave lamination: thick laminates
Thicker laminates maintain a higher pressure compared to thinner ones
Resin flow is associated to resin pressure decrease
Resin flow is promoted by viscosity decrease and is associated to a decrease of the resin pressure
Campbell J. Adv. Mat. 1995
No porosity

## Slide 67
Darcy flow in autoclave lamination: Stress in the fiber stack and resin pressure
Autoclave pressure 9 bar, overbleeding and stiff fiber stack
Heating rate =0.5 oC/min
Bleeder thickness = 0.5 mm
Laminate thickness =4 mm
Thick bleeder and stiff fiber stack
Incomplete filling of bleeder
all autoclave pressure is supported
by the fiber stack
Resin pressure is 0 when viscosity
is not yet at its minimum
Elastic stress=autoclave pressure

## Slide 68: Darcy flow in autoclave lamination: thin laminates
Using additional bleeders (overbleeding) large resin flow is allowed and the fiber stack is deformed up to its limit, i.e. up to a stress equal to autoclave pressure
Gross porosity
Campbell J. Adv. Mat. 1995
zero pressure

## Slide 69: “Alphabet soup” of RTM-type processes
  SQRTM (Same Qualified Resin Transfer Molding)
  The lay up is done with prepregs using aeronautic “Qualified” materials
  A close mold is used. The mold is heated or placed between the heated plates of a press
  The “Same Qualified” resin is injected in order to reach a constant hydrostatic pressure in the mold, the same set for an autoclave cycle.
  - This should dramatically reduce voids using materials developed for autoclave curing.

## Slide 70: Mat preforms for RTM
Advantages
High permeability
Easily infused
Easy handling
Disadvantages
Poor stiffness
Limited strength
No orientation control
Limited fiber volume fractions

## Slide 71: Woven fabric for RTM
Advantages
Balanced properties in the plane of the fabric
Good impact resistance
Good conformability
Disadvantages
Fiber undulation
Asymmetry
Trimming / Handling
UD fabric for RTM
Advantages
Higher stiffness and strength in filament direction
Disadvantages
Poor integrity - "fiber wash" may occur
Anisotropic flow and performance

## Slide 72: Directed fiber preforming

## Slide 73: Braiding
A close profile is obtained with a plain weave with a + q angle
https://www.youtube.com/watch?v=PpIfB_5V5kc&ab_channel=CompositesCentral

## Slide 74: Overbraiding
During overbraiding the preform is fabricated on a core, which has the inner geometry of the desired preform
By reciprocating the core through the braiding point a pre-selected number of layers can be braided
The core is usually removed

## Slide 75: Overbraiding

## Slide 76: Braiding C-frames of A350
A square section is overbraided on a squared section profile and then cut along a mid plane to obtaine two C profiles. The profiles are used in a resin film infusion process.

## Slide 77: Braiding C-frames of A350
The over braided square section is completed with a 0°UD tape and a second braided + q layer (left). Finally a 90 tape is applied (right).

## Slide 78: Braiding C-frames of A350
A) transport system, B) UD tape feeder, C) Braider #1, D) 90° tape winder, E) Braider #2

## Slide 79: Stitching e Non Crimp Fabrics (NCF)

## Slide 80: Multiaxial Non-Woven Fabrics
creel
fibers
Deposition combs
Guiding rolls
Fiber mat bobins
Stitching machine
Stitched multiaxial
collecting rolls
Needle feed chain

## Slide 82
Resin Film infusion stitched preform for aircraft wing panel
Courtesy sigmatex

## Slide 83: Stitched preforms (2D and 3D)
Adv. Composites sept. 2013
Leonardo aerostructures

## Slide 84: Non Crimp Fabrics (NCF): disadvantages of stitching

## Slide 85: Non Crimp Fabrics (NCF): advantages of stitching

## Slide 86: Visual Inspection and Damage Criteria
Typical internal damage from Barely Visible Impact
  Barely Visible Impact Damage (BVID) is defined as damage not found during heavy maintenance surveillance inspections from a viewing distance of five (5) feet, under typical lighting conditions.
Impact Location
Notes: Scale: Line in black box is 0.100 in (2.50 mm)

## Slide 87: Inspection of In-Service Damage
NDI to determine
extent of damage
Visual detection
Repaired
NDI for
post repair inspection
Visual Inspection is the principal method of damage detection
Instrumented NDI required only when visible damage beyond ADL exists

## Slide 88: 787 Structural Health Management Configuration Sensors (eddy current) similar to strain gage in critical points
Cargo and aft service doors (typical)
Fwd cargo door
SHM-007
Sensor locations
Sensors
Aft cargo door
RDC
Sensors

## Slide 89: Preforming methods

## Slide 90: Critical factors in RTM
Fibre impregnation
Viscosity (and its changes) and resin flow
Filling time
Welding lines
Applied pressure (size and cost of molds and presses)
Fabrication of preforms

## Slide 91: Advantages of liquid molding in comparison to open mold processes
Production of large monolithic parts
Good control of fiber content
Possibility of producing sandwich structures and introduce inserts
Good finish on all surfaces for RTM in closed mold
Good control of thickness and dimensional tolerances
Cycle times shorter than those of open mold technologies
Reduced emission of VOC (Volatile Organic Compounds)

## Slide 92: Dry OOA in aeronautic
The MS-21-300 ( Irkut Corp. (Irkutsk, Russia) (160-211 passengers), First flight in may 2017, certification started in the 2019 EASA (European Union Aviation Safety Agency).
First out-of-autoclave (OOA) composite wing and wing box on a commercial aircraft.
The layup is done via placement of unidirectional dry fiber (but with a binder) with automated tape laying (ATL) equipment provided by MTorres (Spain) and Coriolis (France).
The resin (Cytec) is “a unique product that is toughened and infusible without having to introduce tougheners in other forms like films or polymer fibers.”
Further, the resin offers a long window for the infusion process, which provides more than adequate time for large primary structures such as wings. The result, is very low porosity in the final part that “is equal to or less than in an autoclave.”
MS-21 stringers and skins are co-molded in one piece, with the spars and wing box fabricated separately.

## Slide 93: Wind turbine blades
Adhesive bonding extensively used
Notes: Pale eoliche