## Slide 1: Flexible and rigid packaging
Packaging is classified as a function of thickness:
Flexible : 0.01 – 1.5 mm
Rigid : 1.5 – 25 mm
Flexible packaging represents a large part of the market :
ACCESSORIES
47.2%
44.1%
8.7%
FLEXIBILE
RIGIDI
Total transformed plastic materials: 5 106 t
  plastic packaging 3 106 t (60%)
  Recycled (pre and post consumer)
  1.8 106 t
Fonte: Istituto Italiano Imballaggi

## Slide 2: Italian market of packaging materials (tons/1000)
Steel
Cellulose
Wood
Multilayer from converters
Others
Glass
Plastic
Rigid boxes multimaterials
aluminum

## Slide 3: Recycling of packaging materials
2022
2023
2025 forecast
Target 2025 set in 2022

## Slide 4: Food packaging and other
TECHNICAL GOODS
FOOD
46%
OTHER
18%
BEVERAGES
22%
4%
10%
Bakery products
Dry and wet products
Vacuum bagged
Frozen-microwave
Food applications:
REQUIREMENTS
Barrier to gas and vapours
Stiffness and other mechanical properties
Optical properties (transparency, colour)
Dimensional uniformity
Weldability
Printability
COSMETICS AND DRUGS

## Slide 5: Bio-based polymers (world market)

## Slide 6: Bio-based polymers (world market)

## Slide 7
Mass transfer
In the presence of a concentration gradient is observed a mass flow through a polymeric membrane
This happens for example in food packaging and in particular in cases of vacuum or modified atmosphere packaging (MAP=Modified Atmosphere Packaging)
Three steps:
  solubilization (sorption)
  Diffusion
  De-sorption

## Slide 8
Mass transfer under a concentration gradient
It results from casual motion of molecules of penetrant

## Slide 9
Mass transfer (Fickian approach)
I Fick’s law (mass transfer in homogeneous systems):
where:
Jx = diffusive mass flux in direction x, [moli/s m2]
D = Fick’s diffusion coefficent, [m2/s]
C = penetrant concentration
In case there are more penetrating diffusing simultaneously, the flux must be calculated for each species.

## Slide 10
II Fick’s law in 1D: in a plate of thickness e dx surface area A
If the coefficient of diffusion, D, is not dependent on x (and on concentration):
In 3D the balance is :
(It must be completed with B.C and I.C.)
If Henry’s law can be applied (CD = KD a), the equation that describes the mass transfer in a system with known geometry may be derived from a mass balance on a infinitesimal element.

## Slide 11: Typical behaviour
Ideal behaviour where D and S are constant: ideal Fickian behaviour.
Materials in which S and or D depend on concentration. In this case the behaviour is called non ideal Fickian.
Materials in which S and or D are a function of a space coordinate (non-homogeneous materials) or of time (i.e. a glass-rubbery transition occurs during sorption, the polymer structure is changed by the penetrant): Anomalous or Non Fickian behaviour.

## Slide 12: Permeability
The permeability, P, for a gas is defined as:
In steady state the mass flux, Jss, across a polymer film
separating two areas with different concentration
of penetrant, is given by:
Jss=-DDC/l
If Henry’s law holds C=CD= S p:
Permeability correlates the mass flux with the driving force in steady state using the properties in the external phase expressed as partial pressure, activity coefficient or concentration
P in case of ideal behaviour (Fick’s and Henry’s laws hold) is the product of solubility and diffusion coefficients
c1
co
x
l

## Slide 13: Dependence on the temperature
The diffusion coefficient D depends on the temperature according to an Arrhenius like expression:
D=Doexp(-Ed/RT)
Where Ed represents the activation energy of the diffusion process
Remembering that:
S=Soexp(-DHs/RT)
Also the permeability follows an Arrhenius dependence on temeprature
P=Poexp(-EP/RT)
where:
EP=DHs+Ed
Po=SoDo
polymer chains
diffusing molecule

## Slide 14: Dependence on the temperature

## Slide 15: Permeability
The amount of gas crossing a barrier film
in the time t is given by:
Q=Jss A t=P A t Dp/l
Units of measurement of permeablity
Mass flux/pressure gradient=
[M/tL2][L]/[Pressure]=[ML/tL2Pressure]
c1
co
x
l
Material | O2 Permeability (cm3STP mm/m2 day atm) |  | H2O Permeability (g mm/m2 day) | 
PP | 64.2 | T=23 oC | 0.4- 0.59 | T=37.8 oC,90%R.H
LDPE | 132-218 | T=23 oC | 0.39-0.51 | T=37.8 oC,90%R.H
HDPE | 55.9-59.1 | T=23 oC | 0.1-0.12 | T=37.8 oC,90%R.H
PET | 2-3.9 | T=25 oC | 0.71-1.7 | T=37.8 oC,90%R.H
Nylon 6 | 0.61-0.71 | T=23 oC | 5.9-9.8 | T=37.8 oC,90%R.H
Nylon 6,6 | 0.29-0.63 | T=23 oC | 0.23-0.34 | T=38 oC, 90%R.H
PU | 78.7 | T=25 oC | 0.94-3.4 | T=37 oC, 90%R.H

## Slide 16: Permeability
Permeability to oxygen and water of some polymers (O=oriented) (note units)

## Slide 17: Permeability
In food packaging non-ideal behaviors are ignored and the permeability is anyway calculated for the gas of interest; O2, N2, CO2 ed H2O
There is no relationship between molecular size and permeability, in fact, in each polymer, the carbon dioxide proves to be more permeable than the other gases although its molecular diameter (3.4 Å) is higher than that of oxygen (3.1 Å) that it is more permeable than Nitrogen (3.0 Å).
Diffusivity coefficient however depends on the penetrant size
The permeability ratios, called selectivity, are sometimes used to provide an estimate of the permeability of a gas once that of another is known. However this is done with a high degree of approximation (rule of thumb!)
Materiale | O2/N2 | CO2/N2 | CO2/O2
PET PA PVC (not plasticized) LDPE HDPE PS PP (oriented) | 4.4 3.8 3 2.9 3.9 3.8 4.6 | 31 16 25 19 13 30 12 | 7 14.2 8.3 6.5 3.3 7.9 2.7

## Slide 18: Effect of polymer chemistry
The effect of the presence of functional groups along the chain of vinyl polymes is remarkable, being able to vary the permeability of 5 orders of magnitude. This wide range of permeability values is typical of t the materials used for food packaging.
Polar and hydrophilic substituents, in general, reduce the permeability to gases and increase that to water vapor
Substituent in vinyl polymers | Permeability to O2 (normalized values)
-OH -CN -Cl -F -Acrylic -CH3 -phenol -H | 1 4 800 1500 1700 150000 420000 480000

## Slide 19: Multilayer (or laminated) structures in packaging
They combine the different properties of each material and are obtained by co-extrusion (typically up to 5 layers) or by lamination using suitable polyurethane adhesives. This last is done by the so called "converters",
Multilayer structures are optimized considering:
  Costs
  Barrier properties
  Standard requirements (i.e. food contact materials such as PE or use of recycled materials etc.)
  Permeability (gas, vapors and aroma)
  Functionality or ergonomics (i.e. opening features)
  Weldability (better with PE or PP)
  Aesthetics (printability and transparency)
  Processability (i.e. thermoforming of pouches)
  Mechanical properties (tear strength and puncturing strength)

## Slide 20
Barrier properties of multilayer or laminated packaging films is obtained considering permeabilities in series:
Where L1, L2, L3 are the thicknesses and P1, P2, P3 the permeabilities of each layer, respectively
Multilayer structures in packaging

## Slide 21: Technological issues
Fillers: The plastic materials may be mixed with inert fillers, mostly of inorganic nature. Their effect on the permeability is a reduction of diffusion coefficient if the fillers act as a physical barrier (as inorganic they have high density, rigid crystalline lattice and thus low or zero diffusivity) but, sometimes, creating discontinuities and increasing the free volume or defects at the interface, they can instead increase the permeability to gases and vapors. Particularly interesting is the recent use of mineral nanofillers characterized by a high aspect ratio (i.e clay platelets). They are able to drastically reduce the permeability of the matrices in which they are introduced.
Effect of aspect ratio of the filler and orientation

## Slide 22: Semicristalline polymers: homogeneous nanocomposites

## Slide 23: Current Polymer Nanocomposite Technology
Polymer Nanocomposites are composed a polymeric material and a re-enforcing nanoscale material.
The most commonly studied reinforcing nanoscale materials are layered materials, or clays.
Polymer nanocomposites show major improvements in mechanical properties, gas barrier properties, thermal stability, and flame retardancy.
Many factors affect the polymer nanocomposite properties:
  Synthesis method
    Melt Compounding, solvent blending, in-situ polymerization, emulsion polymerization
  Polymer nanocomposite morphology
  Type of nanoparticles and their surface treatments
  Polymer matrix
  Crystallinity, molecular weight, polymer chemistry
.

## Slide 24: TYPES OF NANOPARTICLES
Montmorillonite clays (MMT)
Carbon nanofibers (CNF)
Polyhedral Oligomeric Silsesquioxanes (POSSTM)
Carbon nanotubes (SWNT & MWNT)
Nanographite and graphene
Others (SiO2, Al2O3, TiO2, etc)

## Slide 25
Montmorillonite Clays
Na1/3(Al5/3Mg1/3)Si4O10(OH)2
Na+
Octahedral alumina layer
Tetrahedral silicate layer
Layer thickness is 0.96 nm

## Slide 26: Organic cations (Laviosa, Italy)
commercial name
Dellite HPS
Dellite 67 G
Dellite 72 T
Dellite 43 B
Neat Montmorillonite (MMT)
Organic modified MMT (OMMT)
Notes: A number of TEMs have been examined during this and other nanocomposite studies at SCP.
The small picture in the figure shows the result of particles being sheared to ribbons, stacks of many platelets more than 100nm thick. The ribbons seen in this TEM are common for Case 3 Nanocomposites.
TEM evidence of platelets peeling apart is not common, but has been seen multiple times with a representative TEM shown in the larger picture in the figure..
One of the regions where the platelets are peeling apart from the ribbon is outlined in the TEM.

## Slide 27: Nanocomposite Classification

## Slide 28: Processing Challenge of Nanoclay
8µm Particle >1 Million Platelets
Courtesy of SCP
Notes: SCP provides Cloisite as a powder with a mean of about 8m particle size.
Extrusion is used to melt blend the powder with the resin.
In each particle of powder there are more than 3000 platelets.
The processing challenge is to disperse not only the powder particles but also the platelets.
Dispersion to individual platelets is needed to take advantage of the high aspect ratio (>50) and high surface area (>750m2/gm) of MMT.

## Slide 29: Dispersion Mechanism
Particles
Shear Apart
Platelets Peel Apart
Courtesy of SCP
Notes: This figure continues the proposed mechanism.
Particles of organoclay, with >3000 platelets, fracture to ribbons of intercalants or tactoids. It is proposed this is a results of shearing stacks of platelets apart to make shorter stacks of platelets.
Ribbons reach a size where shearing no longer reduces the ribbon size (the number of platelets in a stack).
Platelets in the ribbons delaminate by peeling apart. This happens after more polymer chains enter the clay galleries and push the platelets further apart. At either some polymer concentration or some platelet separation distance, the platelets peel away from the ribbon to be dispersed as individual platelets.

## Slide 30: Dispersion: Particles Shear Apart - Platelets Peel Apart
Platelets Peel Apart
Particles Shear Apart
Courtesy of SCP
Notes: A number of TEMs have been examined during this and other nanocomposite studies at SCP.
The small picture in the figure shows the result of particles being sheared to ribbons, stacks of many platelets more than 100nm thick. The ribbons seen in this TEM are common for Case 3 Nanocomposites.
TEM evidence of platelets peeling apart is not common, but has been seen multiple times with a representative TEM shown in the larger picture in the figure..
One of the regions where the platelets are peeling apart from the ribbon is outlined in the TEM.

## Slide 31
Polyurethane adhesives for laminated films
Xray Diffractometry(XRD)
2.1%,4.2% and 5.7%vol
Partially Exfoliated
7.1%vol
Intercalated
1.1%,2.2% and 3.7%vol
5.2% and 6.7%vol
Intercalated
Aromatic organic modifier (43 B)
Alifatic organic modifier (67 G)
Partially Exfoliated

## Slide 32
Permeability of polymer nanocomposites
Affect barrier properties Other relevant factors
Tortuosity (aspect ratio)
Volume fraction of filler (reduced transversal area)
Related to orientation
Interphase properties
Nanocomposite synthesis and film production
Basal gap between platelets in omMMT
Bharadwaj Model
Bharadway, Macrom. 2001
FF=nanofiller volume fraction
q
q
Tortuosity orientation
Reduction of transversal area

## Slide 33
Order parameter
Permeability of polymer nanocomposites

## Slide 34
Aspect ratio (W =thickness)
Permeability of polymer nanocomposites

## Slide 35
Changing environmental conditions, a permeability reduction, related to plasticization leading then to non-ideal behaviours, occurs in polymers common used in food packaging (temperature, pressure).
Relative Humidity (R.H.): among other environmental effects, the influence of R.H. on the gas permeability concerns polar and hydrophilic polymers (eg. polyvinyl alcohol, nylon, etilene-vinyl-alcohol EVOH) which tend to absorb moisture which can act as a plasticizer of the structure, greatly increasing the rate of diffusion
EVOH
-[CH2-CH2]n-[CH2-CHOH]m-
EVA
-[CH2-CH2]n-[CH2-CHOCOCH3]m-
effect of environmental conditions and nanofillers

## Slide 36
Nanocomposite O2 barrier (Source: NanoBioMatters)
Nanocomposites EVOH filled with omMMT
Oxygen permeability is reduced of a factor 2 using 4% by weight of omMMT
Permeability is reduced even if measurements are performed in presence of high R.H.

## Slide 37: effect of environmental conditions and nanofillers
NanoSeal barrier coatings developed by NanoPack Inc. are aqueous dispersions of vermiculite platelets in PVOH (Polyvinyl Alcohol) applied to food packaging. The platelets are 1-3nm (nanometers) thick and 10-30µm wide, with average aspect ratio of approx. 10,000:1. These platelets are dispersed in PVOH and aligned in the plane of the coating as a consequence of the shear forces when deposited on a film substrate such as PET, biaxially oriented polypropylene (BOPP), biaxially oriented nylon, or PLA.
NanoSeal coatings are produced as a two component system lightly mixed just prior to application. The parts consist of a carrier resin-additive masterbatch, and water slurry of vermiculite platelets

## Slide 38: Multilayer packaging and R.H. effects
An EVOH layer is introduced to increase the barrier to oxygen (the high polarity of OH groups makes EVOH not affine to non-polar molecules).
However EVOH is affine to water and absorb it during vapour pasteurization, dramatically reducing its barrier properties.
The reduction during time of the content of H2O decreases the permeability of the packaging to O2
High content of H2O (RH)
low content of H2O (%RH)

## Slide 39: Packaging: technological issues
Residual Solvents: they can remain in the polymer as a consequence of the fabrication process or of ink printing or of adhesives used in laminated packaging. They act as plasticizers, leading to a permeability increase.
Plasticizers (i.e. phtalates in PVC or H20 in polyamides). Similar effect than solvents described above
Orientation (mono or bi-oriented films): If the polymer is semicrystalline in nature, the effect of orientation of lamellar crystals on permeability is remarkable. The higher the orientation, the lower the permeability (eg. the bi-oriented PP or BOPP).

## Slide 40: Packaging: technological issues
Polymer blends and copolymerization: many of the structures used for flexible packaging are not obtained by a single type of polymer but derive from the polymerization of more monomers (copolymers) or from the mixture of different resins (blends). The PP used in BOPP films, contains comonomers to improve the process of tentering (biaxial drawing).
Composite and multilayer structures: Almost all packaging is obtained by coupling (eg by coextrusion or lamination) different plastic materials (multi-layer, composite structures). In some cases, film metallization of by evaporation or sputtering (Aluminum), more rarely plasma treatments, is adopted.
Surface modification: food packaging are often modified at the surface to favor the printability and / or adhesion with other films (lamination made by the "converter") using "lacquers” (lacche) or corona treatment

## Slide 41: High barrier biodeg. packaging
Lacquers and metallization are used to improve
barrier properties to oxygen and water vapor of
Polylactic acid (PLA)
Oxygen barrier increases
(cm3/m2/day/bar 23 oC 0% RH)
H2O barrier increases
(g/m2/day/ 38 oC 0% 90% RH)
PLA propylester
Notes: ie

## Slide 42: High barrier packaging
A very high barrier is achieved by metallization with aluminum (about 0.1 microns), but the packaging lose transparency. Residual permeability is due to defects.
Transparent nano-scale coatings based on AlOx ed SiOx (x=non stoichoiometric oxides) are applied by vapour depositions (often on PET). Drawbacks: flex-cracking
Biomedical devices must be sterilized by vapour after packaging is closed. The vapour absorbed by PA and PET increases permeability to O2 and H2O.
Notes: ie

## Slide 43: High barrier packaging
Actis™ coating by Acetylene Plasma .
Vacuum is created inside and outside the bottle
Argon and Acetylene are injected into the bottle
Microwave energy causes argon to reach its plasma state
Acetylene decomposes
Amorphous carbon is deposited on the inner wall of the bottle
Bottle and cavity are returned to atmospheric pressure
Acetylene+argon
air
air
A hydrogeneted amorphous carbon film is obtained (a-C:H) at a growth rate of about 1 nm/s
Ar++C2H2Ar+C2H2+, C2H2++e-C2H+HCH+CHC2+H2
Notes: ie

## Slide 44: High barrier packaging
Actis™ coating by Acetylene Plasma .
Barrier Process | Barrier improvement factors* | 
 | O2 | CO2
Actis™ (Process time 2.2 s) | x 10 | x 7
Actis Lite™ (Process time 1.2 s) | x 3 | x 3
 | O2 Barrier | CO2 Barrier | Solution
Beers, Ciders | X | X | Actis™
Carbonated water |  | X | Actis Lite™
Juices, Teas, Sauces | X |  | Actis Lite™
Notes: ie

## Slide 45: High barrier packaging
Three layers with an aluminium foil (Netstal).
Firstly, a preformed barrier foil made from metal or plastic of low permeability is inserted into the mould. Secondly, the first plastic layer is injected into the outer side of the container followed by a second plastic layer onto the barrier foil on the inner side. The specific structure of the multi-layer barrier compound is such that the barrier foil is protected against damage from the outside without coming into contact with the packaged product. An additional benefit is that in-mould labelling can be used together this packaging
Notes: ie

## Slide 46: Tear strength
  Tear strength must be high for a film used in packaging
  However packaging must be easily opened: a notch is used in a direction parallel to that of orientation to favour tearing
  Peeling of weld line can also be used for opening
Length
Tearing force

## Slide 47: Biomedical packaging: Ethylene oxide sterilization

## Slide 48
Biomedical packaging: sterilization by vapour and gamma or beta radiation

## Slide 49: Food packaging: the use of recycled PET (R-PET)
Recycled polymers must be decontaminated. The reg. CE n. 1935/2004Per reports the so called “challenge tests” to check if washing equipments are capable to remove the pollutant. Virgin PET pellets are polluted with chemicals that simulates the most common ones up to 1000 ppm. Then their release is studied.
  The amount of absorbed pollutant is measured
  The PET pellets are fed to the washing/recycling equipment
  After washing the residual amount of pollutant is measured. Reisdues must be lower than ppb (The test is often performed by the manufacturer washing/recycling equipment)
  The final authorization to the equipment is released by the European Food Safety Authority, Parma
.

## Slide 50: Food packaging: the use of recycled PET (R-PET)
Most recent EU regulations
EU Commission Regulation 2022/1616 contains all the requirements for recycled plastics to be used in food contact. It starts from collection then to decontamination, to applications and to authorizations
“Each Member State shall ensure that from 2025, beverage bottles… which are manufacturedfrom polyethylene terephthalate as the major component (‘PET bottles’) contain at least 25 % recycled plastic, calculated as an average for all PET bottles placed on the market on the territory of that Member State”
“Each Member State shall ensure that from 2030, beverage bottles...contain at least 30 % recycled plastic, calculated as an average for all such beverage bottles placed on the market on the territory of that Member State.”
Three layers bottles virgin/recycled/virgin can be adopted with less stringent prescriptions about decontamination

## Slide 51: Food packaging: the use of recycled PE and PP

## Slide 52: Standards for food packaging
The EC Regulation 1935/2204 requires labeling or information for all substances that may come into contact with food
It authorizes the placing on the market of two types of packaging defined "smart packaging":
  It provides an indication on the freshness of the product: The packaging for example changes color when the product has expired
  It increase the shelf life: the packaging prevents the formation of gases and vapors that can damage the product using for example oxygen or ethylene scavengers.
The regulation prohibits the use of substances that can hide the deterioration of the product (some aldehydes and amines)
The regulation covers all materials (polymers, glass, inks) and the types of packaging including appliances such as coffee machines

## Slide 53: Smart or active packaging

## Slide 54: Smart or active packaging
“Modified atmosphere packaging (MAP) or vacuum packaging are effective until the partial pressure of the oxygen, inside of them, is below a limiting value depending on the type of food.
Gas barrier of the packaging film can be associated with an absorbing substance. Some substances acting as oxygen scavenger absorb the oxygen permeating from outside
  For instance small bags containing ferrous based powders are used. The powders absorb oxygen changing their oxydation level
  oxygen scavengers are often included in laminated multi-layers packaging films

## Slide 55: Gli imballaggi intelligenti o attivi

## Slide 56: Smart or active packaging
Polymeric films based on PET and PP with absorption properties of oxygen are produced by Amoco under the name Amosorb:
  The scavenger element consists of “transition metal, a cobalt salt, catalyzed unsaturated hydrocarbon dienes such as poly-butadiene linked to polyester”
The film includes chemicals that in presence of moisture or UV light, produce radicals, which reacts with the oxygen.
However radicals accelerates the polymer degradation reducing its molecular weight during processing in the melt state. Degradation can also occur during recycling (re-processing).

## Slide 57: Smart or active packaging
EVOH layer ( blue) is not efficient immediately after vapour pasteurization.EVOH absorbs water and its oxygen barrier properties are reduced: “Retort shock”. The oxygen scavenger compensate the barrier loss until EVOH recover its barrier prop.
“Retort pouch”=a heat-resistant bag made of laminated plastic films or foil. It is then heat-sealed and sterilized by pressure cooking in a retort (autoclave) to yield commercially sterilized state of foods.

## Slide 59
Fruits & Vegetables Types | Rate of Ethylene Production | Level of Ethylene Sensitivity | Principal reaction to Ethylene Gas
Apples Apricots Asian Pears Asparagus Avocados Bananas Berries Broccoli Brussel Sprouts Cantaloupe Carrots Cherimoya Cherries Cucumbers Eggplant Grapefruit Grapes Kiwifruit Lemons, Limes Lettuce (*2) Mangoes Melons (*3) Nectarines Onions, Garlic Oranges Papaya Passion Fruit Peaches Pears (*5) Persimmons Plums, Prunes Potatoes (*6) Quinces Tomatoes Watermelons Floral & Nursery Commodities Carnations -Cut Roses -Cut Flower Bulbs Nursery Stock | VH H H VL H M L VL VL H VL VH VL L L VL VL L VL VL M M H VL VL H VH H H L M VL L M L VL VL VL VL | H H H M H H L H H M L H L H M-H M L H M H H H H L M H H H H H H M H H H H H H H | Scald (*1) Decay Decay Toughness Decay Decay Mold Yellowing Yellowing Decay Bitterness Decay Softening Yellowing Brown Spots Mold Mold Decay Mold Russet spotting Decay Decay Decay Odor, sprouting Mold (*4) Decay Decay Decay Decay Decay Decay Sprouting Decay Shrink, decay Lose firmness Sleepiness (*7) Prem. opening Shrink (*8) Slower start
VL = Very low, L = Low, M = Moderate, H = High, VH = Very High *1. Lose crunch *2. Leafy greens *3. Crenshaw, Honeydew, Persian *4. Rind breakdown *5. Anjou, Bartlett, Bosc *6. Processing, Seed *7. Leaf curl *8. Retards flower formation |  |  | 
The need of ethylene scavengers

## Slide 60: Smart or active packaging
Smart packaging can be characterized by antimicrobial properties mainly according to the following approaches :
  Binding an enzime or proteins with antimicrobial properties on the internal side of the packaging
  The packaging release an antimicrobial agent or subtract to the food a key component needed for microbial growth
An example of this last mechanism is given by the inclusion in a packaging film of microporous zeolites particles. Zeolite was formerly “loaded” with silver, that released in form of ions in solution, is capable to prevent bacterial growth.

## Slide 61
Bacteriostatic efficacy evaluation

## Slide 62
Neat Cotton fibres
Efficacy not suffcient
Bacterium growth is extended to all the plate including the areas closer to fibres
Bacteriostatic efficacy evaluation

## Slide 63
Well defined area of inhibition to bacterial growth
Bacteriostatic efficacy evaluation
Cotton fibres treated with silver
Good efficacy

## Slide 64
Bacteriostatic efficacy evaluation
Cotton fibres impregnated with antibiotic
Good efficacy
Well defined area of inhibition to bacterial growth- This area is smaller than that found using silver

## Slide 65: Smart or active packaging
Maxwell Chase Technolgy sells in USA trays and pouches Fresh R-pax containing a gel capable to reduce the moisture content and the consequent bacteria growth :
  Highly absorbent (a gel) food safe material which is built into Pads, Pouches and Trays
  Traps moisture and retains it even under pressure
  Removes and retains food spoilage bacteria (i.e. Salmonella, escherichia coli etc.)
  Keeps product fresher and safer - significant extension of shelf life of fresh cut fruit and vegetables

## Slide 66: Smart or active packaging
Emission of CO2
Carbon dioxide-emitting sachet and label devices can either be used alone or combined with an oxygen scavenger. An example of the former is the VerifraisTM package, manufactured by Codimer sarl (Paris, France), which has been used for extending the shelflife of fresh meats and fish.
This innovative package consists of a standard MAP tray but has a perforated false bottom under which a porous sachet containing sodium bicarbonate/ascorbate is positioned.
When juice exudate from modified atmosphere packed meat or fish drips onto the sachet, carbon dioxide is emitted and this antimicrobial gas can replace the carbon dioxide already absorbed by the fresh food, thus avoiding pack collapse.

## Slide 68: Smart or active packaging
Packaging can be used to cool down or heat up a beverage or a food
An example of food heating is given by a capsule containing CaO that can put in contact with water by the user when he decides to heat up the food or the beverage
The reaction CaO+H2OCa(OH)2 is strongly exothermic so generating the heat necessary to heat the food or the beverage.