## Slide 1: A possible definition
When different materials are combined the resulting composite materials can be characterized by properties very different from those of constituents.
The nature develops structural materials (bone and wood for instance) by “self assembly” depending on the loads applied during growth
Bone: hydroxyapatite (stiff) + collagen (tough)
Wood: cellulose crystals (stiff) + amorphous lignin (tough)

## Slide 2
specific modulus (108 cm)
specific strength (106 cm)
Specific properties of fibers

## Slide 3
Specific properties of composites
Specific modulus

## Slide 4
Composite design chart

## Slide 5
Composite design chart

## Slide 6
An Interpetration of the specific strength
Load capacity (lbs) of a cylinder 1 ft long that can be purchased for1 $
Using 1$ I can purchase a cylinder of 1 ft , weighing 1 lb, characterized by a higher strength depending on its volume. At a higher volume corresponds a higher section area at fixed length when the materials is characterized by high strength and low density.
The cost per lb plays also a key role
1 ft

## Slide 7
A brief story of composite materials
Prehystory
  Use of wood as a natural composite, straw in bricks
1800. Steel rebars in concretes
1910 . Reinforcement in phenolic resins made of natural fibers and asbestos
1938-1945:
  Epoxy resins reinforced with glass fibers (Owens-Corning Fiberglass Corporation) use in electric insulators
  First GFRP (Glass fiber reinforced plastics) used on boats and air vehicles
1946: Patented Filament winding for the fabrication of pipes and tanks
1961 First production of carbon fibers
1963 First production of boron fibers
1968 Horizontal stabilizer of F-14 made of epoxy resin reinforced with boron fibres
1973 First production of aramide (Kevlar) fibers
70s and 80s large use of composites in sport goods and as secondary structures in airplanes
90s application of composites in primary large areonautic structures and in several industrial applications inclusding automotive
2008 Production of the first large (>300 seats) airplane with a carbon fiber fuselage
2012 Space launcher in carbon fiber composites VEGA from Avioaero

## Slide 8: Why a composite material is needed
High ratio strength/density and modulus/density (high specific properties: higher than those of metals)
Anisotropy of properties can be used to optimize the weight: not only a component is designed but also the used material
High corrosion resistance. In general, higher “durability” in environment critical for metals
Electric insulation when glass fibers are used (E-glass)
Small productions of objects with complex shapes at low fix cost (moulds) in comparison with metals or plastics.
Integration of many components in a single composite parts (in comparison with equivalent shape made using metals, for instance)-Boeing estimates a 19:1 part count reduction, where composites replace aluminum

## Slide 9: Wind Turbines. Typical blade length 25-80 m Advantages: monolithic structures of complex shape, durability for 20-25 years 200 GW installed in 2010, 600 GW in 2019
Wind energy is the largest consumer (by mass) of global carbon fiber at more than 23,000, metric tonnes. With wind energy forecast to triple again by 2030 and grow fivefold by 2050.
Two-pieces blades for onshore applications under development.
2021: Vestas announces 15 MW Offshore WT. Each blade on the V236-15.0 MW measures 115.5 meters (379 feet) long, giving it a total height of 261 meters

## Slide 10: Wind blade structure
A structural spar and two shells are separately built. Then the two shells are adhesively bonded to the spar. A sandwich structure is preferred for shells. Extensive use of adhesives
Shells play a structural role in the middle part of the section. Two (ore one) shear webs are added by adhesive bonding. Extensive use of adhesives

## Slide 11
Composites Technology 2010, vol 17, n°2, p 24

## Slide 12
sports equipment:
bikes, fishing rods, golf clubs, tennis racquets, skis, snowboards
Notes: Trek bike
Maximum strength-to weight ratio Frames made with Hexcel carbon Prepreg weigh just 1.11 kg, but are incredibly strong.

## Slide 14
Glass fibers in boat up to 75m
Carbon fibers in race boats
Laminated sails includes high performance reinforcements
Main advantage: complex shape monolythic structures

## Slide 15: 70 m ship for the Swedish navy. Use of glass and carbon composites

## Slide 16: Trimaran made with natural fibers
Gwalaz is a 23.5ft trimaran that will be built with flax fibres and cellulose, cork and balsa wood and bio-sourced resins.

## Slide 17
Railway vehicles
Advantages: small series, complex shapes
Requirements: fire resistance

## Slide 18
Metro Train (CG Rail, Chinese-German Research)
Cetrovo 1.0 features carbon fiber for its main load-bearing structures, as composite content exceeds 70%:
composite front cabin, car body, underfloor paneling and bogie frame.
developed and produced Cetrovo’s carbon fiber bogie crossbeam component
Weight saving compared to metal solution 11%
Expected energy saving between 7% and 15%
Expected 22% savings of maintenance costs

## Slide 19
Materials in automotive applications. Composites?

## Slide 20
1941 Ford Hemp Car
From Popular mechanics: “70 percent of cellulose fibers from wheat straw, hemp and sisal plus 30 percent resin binder. The only steel in the car [was] its tubular welded frame.”
More recently:
Trabant (east germany)
Citroen Mehari (1960-70)

## Slide 21
Automotive applications (short fiber)
Long fiber (discontinuous)
Trunk floors, Trunks, Bumpers, Truck side panels and spoilers etc.

## Slide 22
Electric vehicle by BMW and SGL carbon fibers: BMW i3
carbon fiber passenger cell

## Slide 23
Alfa Romeo 4C mono-coque
carbon fiber passenger cell (four parts)

## Slide 24
Supercars
Lamborghini sesto elemento (sixth element),

## Slide 25
Mass production vehicle by BMW and SGL carbon fibers: BMW -7
carbon fiber composites parts

## Slide 26
Mass production vehicle by BMW and SGL carbon fibers: BMW -7
carbon fiber-aluminium hybrid construction of passenger cell

## Slide 27
Perspectives for applications in cars: 2021 targets
Average data for each car manufacturer: only fleet average is regulated
Heavier are allowed higher emissions,

## Slide 28
Perspectives for applications in cars
(average gCO2/km for each carmaker, depending on average weight)
Since 2010 the emissions have been 170 gCO2/km
Target 2015=120-140 gCO2/km
By 2021 the emissions are 90-100 gCO2/km
By 2025 until 2029 the emissions must be 80 gCO2/km and then 60 gCO2/km
From the fig. about 8.5-10 gCO2/km are saved for each 100 kg of weight saved
Trend: start now with medium-sized market productions very soon
Vehicle mass, kg
gCO2/km

## Slide 29: Lifecycle emissions: Elife-tot/Slifetime
Renewable and Sustainable Energy Reviews 159 (2022) 112158
(Elife-tot=total life-cycle emissions)

## Slide 30
Perspectives for applications in cars: trend of cars weight

## Slide 31
Old motorbike applications:Vincent HRD “Black Knight”
Fairings made of glass fiber reinforced plastic

## Slide 32
Advanced motorbike applications:Ducati 1299
Swingarm (monocoque, wheels and rear subframe)
RIBA Composites-Faenza-Italy

## Slide 33
Biomedical applications
Limb Prosthesis and socket
Kaiteki Institute –Japan and Otto Bock
Glass fiber reinforced composite
Carbon fiber reinforced composite
Adv.: low weight, taylored stiffness, fatigue resistance

## Slide 34
Esoskeleton devices
The new carbon fiber frame has dramatically reduced the weight of the exoskeleton from 6 kg without the battery to 4.5 kg
esoskeletonreport.com

## Slide 35
Radiolucent and surgical tables
carbon fiber tables, light and transparent to to X-Ray and ionizing radiations
Steris.com

## Slide 36
Oil and Gas exploration

## Slide 37
Oil and Gas exploration
spoolable umbilical reinforced with carbon fibers rods
Installed in Gulf of Mexico 2700 m deep water

## Slide 38: Robot arm
The KUKA KR 100-2 PA four-axis robot's third axis linkage is made of carbon fiber composite material. This state-of-the-art material makes the robot light without sacrificing high stiffness.

## Slide 39
Aluminum Conductor Composite Core (ACCC)
It is lighter. The weight saved can be used for more aluminium conductor.
Softer, fully annealed aluminium can be used for the conductors. Standard cable uses harder aluminium which contributes to the cable's tensile strength, but has about 3% less electrical conductivity.
It has a much lower coefficient of thermal expansion (CTE) . This lets the cable be operated at a significantly higher temperature without excessive sag between poles.
The first two factors result in roughly 30% greater conductivity than an equivalent ACSR conductor, allowing 14% more current to be carried at equal temperature

## Slide 40
Lift cable from Kone (Ultrarope)
The biggest limiting factor in building higher until now has been the steel rope weight – and we have reached the limit of that technology at 500 metres.
Comprised of a carbon fiber core and a unique high-friction coating, KONE UltraRope is extremely light, meaning elevator energy consumption in high-rise buildings can be cut significantly.
Since 2010, it has been tested in operation at the world's tallest elevator testing laboratory, KONE's Tytyri facility built over 300 meters underground adjacent to an active limestone mine
Installed at Singapore Marina Bay Sands Building in a195 m tall lift

## Slide 41: Furniture and appliances
Revology chair. Natural flax fibers as reinforcements and a crop based bio-derived resin (available 2017)
http://http://revology.com/
Shower and sink
http://designcarbon.wordpress.com/

## Slide 42: Civil applications (retrofitting)
Retrofitting of chimney
Retrofitting of poles and bridges
GFRP roof Santa Maria Paganica (L’Aquila)
Notes: http://www.yes-mks.co.jp/en/carbon/use_02.html

## Slide 43
Harbour poles
Pedestrian Bridge 63 m
GFRP+Aramid cables
(Scotland 1992)
Handrail, ladders
Civil engineering applications (new buildings)
Bridge 27 m long 5M wide in Germany
(GFRP deck on metal beams)
Notes: http://www.yes-mks.co.jp/en/carbon/use_02.html

## Slide 44: Civil engineering applications (new buildings)
The 52-meter-high artwork of Rita McBride was named for its waisted shape of Mae West. A new Tram will run through it below.
It is made of carbon fibers tubes Installed in Munich, Germany on 04 February 2011
Notes: http://www.yes-mks.co.jp/en/carbon/use_02.html

## Slide 45: Other applications
RF ground antenna
(EM transparency)
Industrial rolls
CF violin Guitars Harp
Notes: http://www.yes-mks.co.jp/en/carbon/use_02.html

## Slide 46: Carbon Fiber Flying dress by Lady Gaga (Volantis)
https://www.youtube.com/watch?v=RjrhxNsxq60
Notes: http://www.yes-mks.co.jp/en/carbon/use_02.html