## Slide 1
Mass Diffusion in polymers
Controlled release of drugs and biomedical appl.
(filtration, dialysis contact lenses etc)
Environmental resistance of polymer and composites
Barrier materials for packaging
Other applications(fuel cells, separation membranes)
Outline:
Equilibrium conditions between a penetrant and a polymer: analysis in steady state (sorption)
Kinetic of diffusion and steady state diffusion (permeability)

## Slide 2: Controlled Release of drugs
Limit of toxicity
Conventional drug supply Single dose in controlled release
Time
Time
Limit of efficacy
drug concentration in the blood of a patient

## Slide 3
PHENOMENOLOGICAL MODELS FOR PENETRANT SORPTION
Polymer-penetrant interaction at equilibrium
Polymer and penetrant interact like a solvent and a solute
sorption isotherms: plots reporting the amount of penetrant (gas or vapour or liquid) absorbed at constant temperature as a function of partial pressure (or activity or concentration) of the penetrant.
The typical behaviours of a polymer can be :
  sorption according to ideal behaviour typical of liquids (Henry’s law)
  Non-ideal behaviours
    Adsorption mechanism on walls of pores are involved: Langmuir isotherm
    Specific interactions polymer/penetrant or polymer plasticization: Flory-Huggins isotherm
    Specific interactions polymer/penetrant and microporosities: BET (Brunauer–Emmett–Teller) isotherm

## Slide 4
The solubility (S) at equilibrium of chemical species in a polymer depends on:
Physical state of the polymer (semi-crystalline, glassy, rubbery)
Eventual interaction between polymer and penetrant
• Ideal behaviour (Henry’s law): rubbery polymers (they behave like low molecular weight liquids)
sorption isotherms follow a linear dependence on external activity
CH=S a Eq. 1
CH = Concentration of penetrant in the polymer
a= external activity coefficient for vapours or partial pressure for gases (CH=S p)
      The coefficient S represents:
            Henry’s constant (for gases)
            Moles of penetrant in the polymer volume at standard conditions for vapours
            If Eq. 1 is re-written as a function of external concentration CE CH=S CE it is dimensionless and S represents a partition coefficient
Sorption isotherm

## Slide 5
Henry’s constant (S in eq. 1) is a true constant only in the ideal conditions
        p (or a or C)
If a (or C) is used, being a dimensionless S has the physical dimensions of a concentration.
S has the physical dimensions of mole/Joule when partial pressure are used at the II member of eq. 1 (Sp).
The SI units are in this case: mole m2 mole
        ---------- = --------
        N m3 J
Sorption isotherm
CH

## Slide 6
However, very often the solubility is expressed in units of measurement that takes into account the different nature of the variables used in the case of gas (CD=S p):
For simple gases S is expressed in cm3 (STP)/ cm3 / bar .
The conversion to S.I. is: 1 cm3 (STP)/ cm3 / bar = 10-5 cm3(STP)/cm3/ Pa
1 cm3 of PE (density=0.92 g/cm3) contains np=0.92/28=3.3 10-2 moles of repeating units
1 cm3 of gas (STP, 1 bar, 25 oC) contains n=PV/RT moles
nA=101325 10-6/(8.314*298)
nA=4.1 10-5
If N2 solubility S=0.025 then np/nA=32000
i.e. 32000 repeating units of polymers for each gas molecule.
This ratio must be corrected considering only the amorphous phase in semicrystalline polymers
(1-Xc) = amorphous fraction
Xc of HDPE about 0.65 so
np/nA(1-Xc)=32000*0.35=11200
Sorption isotherms

## Slide 7
S in many cases in not a constant and depends on:
Nature of penetrant and in particular the type of molecular interactions that exist between the molecules of the penetrant
Temperature: S=Soexp(-DHs/RT) where the sorption enthalpy DHs=DHc+DHM is given by:
  DHc= molar heat of condensation. This term is close to 0 for gases while is high for vapours.
  DHM=Molar enthalpy of mixing= enthalpy change observed when one mole of a penetrant A in the liquid state is added to a mixture A-polymer of predetermined composition. This term depends on both the AA interactions and those polymer-polymer when compared to those A-polymer.
Sorption isotherms

## Slide 8
S can be measured at tifferent temperatures and the sorption enthalpy is obtained from an Arrhenius plot:
The sorption enthalpy is obtained from the slope of the linear fitting of experimental data
lnS
1/T
Sorption isotherms

## Slide 9: Solubility parameter
The solubility parameter is a measure of the intensity of intermolecular secondary bonds
For a low molecular weight solvent :
Cohesive energy density (CED)=DEv/Vl e DEv=DHv-P(Vv-Vl)
DHv= Molar heat of vaporization
P= vapour pressure
Vvand Vl = Molar volume of vapour and liquid phase
Solubility parameter

## Slide 10: Solubility parameter

## Slide 11: Sorption enthalpy and Solubility parameter
Assuming that in the ideal solutions there is no change in the volume as a consequence of mixing: DVM=0
Mixing free energy (solubility when >0), DGM :
  DGM=DHM-TDSM=DEM+PDVM-TDSM=DEM-TDSM and therefore DHM=DEM
DEM can be expressed as a function of intermolecular bond energies and therefore of vaporization energies:
vAe vP= volume fraction of penetrant and polymer
VA e VP= Molar volume of penetrant and polymer
The solubility parameter is (DE/V)0.5 therefore:
DHM=V vA vP(dA-dp)2

## Slide 12: Sorption enthalpy and Solubility parameter
DHM=V vA vP(dA-dp)2 can be zero if the solubility parameters of penetrant and polymer are the same otherwise the sorption process is (almost) always endothermic
On the other hand, the mixing entropy is always >0: This term makes DG<0 and therefore makes the mixing possible
However, in a very limited cases it is also possible a negative (exothermic) value of the mixing enthalpy. This can occur when very strong specific polymer-penetrant interaction occurs:
  Polymer structure is changed by the penetrant
  Presence of molecular size pores. A special case is given by clathrates=organic crystals (also macromolecular) that trap molecules in an interstitial position.

## Slide 13: Sorption enthalpy and Solubility parameter
In the case DHM is different from 0, Flory and Huggins introduced the interaction parameter c:
    DGM= RT[nAln(vA)+npln(1-vA)+ c nA(1-vA)]
    DSm ideal solution (a quantity <0)
  nA, np, number of moles of penetrant and polymer
cRT represents the interaction energy per mole of solvent for a given couple polymer-solvent
  ≅ 0.34+ (dA-dp)2 VA/RT
  c=Flory interaction parameter, VA= molar volume of penetrant
c <0.5 the polymer (amorphous and linear) is soluble
c =0.5 represents the solubility limit and the temperature at which c =0.5 is called Flory q temperature and the solvent at that temperature is called Flory q solvent.

## Slide 14: Solubility parameter
the solubility parameter is measured adopting a comparison procedure. A weakly crosslinked polymer is used to prevent full dissolution
In order to measure the solubility parameter of a polymer (dp), the polymer is placed in contact with several different solvents and then the amount of absorbed solvent, m, (or the swelling Q= (m-m0)/m0rs) is measured.
  m and m0= weigth of swollen polymer and initial polymer weight
  rs=solvent density
Q
d
dp
The solubility parameter of the polymer is taken equal to that of the solvent that produces the maximum swelling (highest quantity absorbed)

## Slide 15: Solubility parameter

## Slide 16: Solubility parameter
Nylon 6

## Slide 17: Solubility parameter
Solubility parameter is the result of the contribution of different type of secondary non-covalent bonds:
d2=d12+d22+d32=polarity+ H bonding + Van der Waals or dispersive bond

## Slide 18: Calculation of Solubility parameter
When dealing with polymers of known molecular configuration d can be obtained from:
G= Molar attraction constant
r=density
M=molecular weight of repeating unit

## Slide 19: Calculation of Solubility parameter
Polystyrene r=1.05 g/cm3 M=104 g/mole
d=1.05 (133+28+735)/104=9.05 (cal/cm3)0.5
[G]= cal0.5 (cm3) 0.5 /mole

## Slide 20: Polarity of polymers
Solubility parametr or surface energy
PTFE
SILICONI
PP
PE
TPO
EPDM
SBR
PS
PVC
PMMA
Polyester
PC
epoxy
PU
PA
TPO Thermoplastic olefin
EPDM Ethilene-propylene-diene monomer
PC Policarbonate
PU polyurethanes
PA polyamides

## Slide 21: Complex sorption isotherms
Fig I: Ideal behaviour described by Henry law.
Fig. II: It is the Langmuir isotherm; This behaviour occurs when penetrants are hosted in microporosities.
Fig III: Flory-Huggins isotherm; In this case the solubility coefficient increases with external partial pressure: plasticization occurs
Fig IV: Two stage Brunauer-Emmet e Teller (BET) isotherm: it results from the sum of microporosities and plasticization (sum of dashed curves or case II and III)

## Slide 22
Langmuir isotherm for glassy polymers (T < Tg)
A simple linear relationship does not adequately describe the sorption when T<Tg. A polymer in the glassy state may in fact be considered at the same time:
A liquid. In this case the molecules of penetrant occupy very small interstitial sites, about the same size of a molecule of penetrant).
A porous solid. Part of the sorption is related to a phenomenon similar to that occurring in pore surfaces of zeolites or activated carbon. This similarity arises from an excess of free volume in glassy polymers, frozen as microcavities (1040 Å). These are stable in absence of rotational mobility of chain segments so determining an excess of free volume than expected from a diagram v-T (considering the equilibrium state as the extrapolation of specific volume at the liquid state).
The phenomenological model that describes the sorption process must take into account both mechanisms

## Slide 23: Glass Transition as a second order transition
Discontinuity of dv/dT (Coefficient of Thermal Expansion, CTE, once divided by the initial volume)
Discontinuity of dh/dT (specific heat, Cp or Cv)
The glass transition can be considered a second-order transition
Tg is obtained as a limiting value for experiments conducted by cooling at “infinitely” low rates
Tg as a transition to a metastable state
The glass transition temperature, in this case, represents the temperature at which the characteristic relaxation time of the rotational mobility of the main chain is of the same order as the time scale of the experiment
The glassy and liquid (or rubbery) states constitute a single thermodynamic phase
This explains why different Tgs at are observed when the heating or cooling rates vary
It is also possible to justify the elastic behaviour that polymer melts show and the viscous response of polymer glasses, under particular stress conditions (time scale)

## Slide 24: Tg as an iso-free volume transition At T<Tg free volume is “frozen”
free volume in excess
frozen microcavities
polymer matrix according to equilibrium specific volume
Extrapolated specific volume at equilibrium: VA
Specific adsorption sites on the microcavity wall
adsorbing surfaces

## Slide 25: Glass Transition as an iso-free volume transition
Free volume. Viscous flow at T>Tg (liquid) is allowed by jumps of chain segments in vacancies or voids (“holes”)
By reducing the temperature when the polymer state is liquid or rubbery, the number of voids (the free volume of the order of a nanometer size) is reduced and this causes the reduction of the specific volume
At Tg the position of these holes is frozen and the polymer becomes “glassy”
When cooling from the melt, at the glass transition, the free volume is constant (iso free volume transition) for all polymers (about 2.5%) and does not decrease anymore
With this interpretation the mechanisms of gas and vapor absorption in glassy polymers are explained.
During cooling at glassy state the “occupied” volume reduces generating an excess of free volume. This correspond to a lower CTE in the glassy state compared to that in the rubbery state

## Slide 26: Sorption isotherms for PET-CO2
The isotherms presents a non-ideal behaviour at T<Tg and ideal at T>Tg
T<Tg
T>Tg

## Slide 27
Sorption in microcavities (Langmuir isotherm)
In the case of a single layer of adsorbed molecules at cavity walls:
CL= concentration of adsorbed penetrant at cavity walls
C’L= Saturation constant of cavities :
    for p¥ CL C’L
    if C’L is constant, the penetrant does not change the polymer structure
    b = affinity constant of adsorption in the cavities
CL
P (or a)
C’L

## Slide 28
Langmuir isotherm
This expression is obtained in the hypothesis of dynamic equilibrium between adsorbed and de-adsorbed molecules in the microcavities. Indicating:
  S=number of adsorbing sites
  S1= number of adsorbing sites occupied by penetrant molecules
  So=S-S1= number of adsorbing sites still available
The rate of adsorption is dependent on p: K2pSo=K2 p(S-S1)
The rate of de-adsorption is assumed not dependent on p : K1S1
The penetrant reaches the equilibrium concentration in the polymer when :
K1S1=K2 p(S-S1)=K2 pS - K2 pS1
Extracting the common factor S1:
S1(K1+K2 p)=K2 pS
and taking F=S1/S it is obtained:

## Slide 29
But F=S1/S = CL/CLmax and then :
The meaning of C’L e b is obtained comparing this eq. with the last of previous slide:
=
C’L=CLmax and then C’L represents the capacity of adsorption sites expressed with the same units of CL [cm3(STP)/cm3polymer]
b = K2/K1 = (“rate” of adsorption)/(“rate” of de-adsorption)
The highest b the highest is the affinity of the adsorbed molecules with the adsorbing polymer, i.e. the affinity between the microcavity in the polymer and the penetrant.
Langmuir isotherm

## Slide 30
Dual Sorption Model: Langmuir’s iotherm + Henry’s isotherm
CH
CT
Sorption in the bulk: mixing
Adsorption on the surface of frozen microvoids
CH=Sp
CH
CL’
CL
CT

## Slide 31
I
II
Part I (low pressure, bp<<1)  CT= (S +C’Lb)p = tand p (*)
Part II (high pressure, bp>>1 )  CT= S p + C’L = tang p+ C’L (**)
d
g
A
Dual Sorption Model: Langmuir’s isotherm + Henry’s isotherm

## Slide 32
At low p Langmuir’s mechanism is dominant. Cavities are not yet saturated and tand = (S +C’Lb).
As p increases microcavities saturate and Henry’s linear behaviour becomes dominant
Dual Sorption Model: Langmuir’s + Henry’s Isotherms
        Two slopes (tand e tang) and one intercept (C’L) are obtained when the equations are simplified for low and high p: using these values the three parameters needed for the dual sorption behaviour can be obtained.
        Besides KD (or K in the former pages) also b depends on the temperature :
b=boexp(q/kT)
q=heat of adsorption in the microcavities.
k= Boltzman constant

## Slide 33
Thermoplastic poly-imide (Kapton)
Dual Sorption Model: Langmuir’s iotherm + Henry’s isotherm
S
CL’

## Slide 34
When sorption temperature approaches Tg the contribution of microcavities, i.e. frozen free volumes (Langmuir), is reduced: and hence C’L0 and the shape of the curves changes becoming linear (Henry)
Dual Sorption Model: Langmuir’s iotherm + Henry’s isotherm
Rigid amorphous fraction (Xra) is responsible of C’L>0 for T>Tg
Xra =1-Xc- Xa Usually not 0!
Xa = amorphous fract.
Xc Cryst. Fraction

## Slide 35
Flory-Huggins Isotherm
If there are not strong specific interactions, the isotherms are characterized by an upward concavity at high pressure (or activity), after an initial linear (rubbery polymers). In this case the polymer structure is changed by the penetrant as p (or a) increases  the solubility coefficient depends on p (or a).
S is a function of vA.
vA is the molar fraction of penetrant, VA the molar volume and c the Flory interaction parameter, not dependent on a.
CFH
a (opp. p)

## Slide 36
Dual Sorption Model: Flory-Huggins+Langmuir’s isotherm
If there are strong specific interactions (for example OH groups in the polymer and water or alcohols as penetrant) isotherms may have a concavity facing upwards even at low p. Also in this case a rubbery polymer is modified in its structure from penetrating the solubility coefficient depends on p (or a).
CL’
CFH
CH
CT
= BET
CL
C’L
If the polymer is glassy and there are also specific interactions, the two behaviors, Flory-Huggins and the Langmuir isotherm are combined resulting in the Brunauer-Emmett-Teller (BET) isotherm

## Slide 37
\
Example: water sorption in a strongly hydrophilic glassy polymer: an ester of hyaluronic acid
activity
Penetrant volume fraction
CL’

## Slide 38
Semicrystalline polymers
For semicrystalline polymers the crystalline phase is considered impervious to thepenetrant molecules: sorption occurs only in the amorphous phase
PET
Xa *100 (% amorphous polymer by WAXD)
Solubility

## Slide 39: Summary
Rubbery polymers
  Sorption of gases and vapors at low pressures and activities respectively: Henry’s law
  Sorption of gases and vapors at high pressures and activities respectively with no specific interaction: Flory-Huggins isotherm
  Polymer and penetrant are chemically affine (i.e. water in hydrophilic polymers): Complex isotherms, such as Flory-Huggins + Langmuir)
Glassy polymers
  Sorption of gases at low pressures: Henry+Langmuir
  Sorption of gases at high pressures or sorption of vapors : Fl-H+ Langmuir
  Polymer and penetrant are chemically affine: Complex isotherms, such as Flory-Huggins + Langmuir)
Semicrystalline polymers
  Sorption in the amorphous phase according to the former cases 1 and 2

## Slide 40: The special case of syndiotactic polystyrene: sorption of organic solvents in semicrystalline polymers.
Clathrate structure with Di-Chloro-Ethane (17, 18) in the cavity of elementary cell of synditactic polystyrene (“empty d” form)

## Slide 41
The crystalline structure called “empty-d” is characterized by a high sorption at low activities in the cavity present in the crystalline structure
The comparison with the other curves indicates that the sorption in the amorphous phase is lower.
When the cavities in the crystalline phase are saturated, then sorption becomes significant in the amorphous phase as activity increases
The special case of syndiotactic polystyrene: sorption of organic solvents in semicrystalline polymers.

## Slide 42: The special case of syndiotactic polystyrene: sorption of organic solvents in semicrystalline polymers.
Sorption at low activity (in figure partial pressure) is characterized by a downward concavity indicating that there are microcavities that are approaching saturation