## Slide 1: Polymer Matrices
Thermoplastic Matrices
Linear or branched molecules held together by weak secondary bonds.
They can be fused and processed several times.
Thermosetting Matrices
Molecules linked by strong covalent bonds forming a three-dimensional network.
They can not be melted and reprocessed by heat but for T>Tg they behave like a rubber.
Thermoplastic
Thermosetting

## Slide 2: Polymer Matrices: thermosetting
Thermosetting Matrices
During composite manufacturing they are used as low viscosity monomers or oligomers, which react irreversibly to form a highly crosslinked structure. After reacted, the polymer is no longer reformable and can be processed only once.
Features:
Fluid resins that harden due to the temperature
Stiff and brittle after curing reaction (polymerization)
During processing a chemical reaction takes place (irreversible process)
Highly exothermic reaction accompanied by volume reduction (shrinkage)
Amorphous
Long processing times to achieve complete crosslinking
Degrade without melting
Absorb moisture or solvents but they do not dissolve
Dimensional stability (it doesn’t flow upon heating)
Mechanical properties dependent on the degree of crosslinking
Advanced thermosetting : stability at very high temperature, resistance to thermo-oxidation
Notes: 2

## Slide 3: Polymer Matrices: thermoplastic
Thermoplastic Matrices
During composite manufacturing they are used as high molecular weigth polymers
that can be melted for the fiber impregnation and then cooled.
Features :
Fast processing (there is no curing).
Their processing requires high temperatures and pressures due to their high viscosity.
They can be re-melted through multiple forming and assembly (recycling and welding).
Amorphous or semi-crystalline solids that soften or melt due to the temperature
Reversible physical process
High molecular weight
Toughness
Poor dimensional stability (high creep, effect of solvents, they can flow upon heating)
Shrinkage after molding
Mechanical properties dependent on the molecular weight
Advanced thermoplastics: strength to high temperature, creep resistance, resistance to solvents
Notes: 3

## Slide 4
Thermosetting Matrices
Advantages :
Low viscosity (good fiber impregnation)
Thermal stability
Chemical resistance
Low creep
Thermoplastic Matrices
Advantages:
High fracture toughness
High strain at break
Unlimited storage time at room temperature
Short manufacturing time
Easy repair by welding or solvents
Post-forming
Disadvantages:
High viscosity in the molten state
High creep
Low thermal
stability
Disadvantages:
Limited storage time at room temperature
Long manufacturing time in the mold
Low strain at break
https://drive.google.com/file/d/1hN6yz91LUoF4P4Ia7yqndUEz-PhH8CjN/view

## Slide 5: Thermoplastic polymer matrices
High performance polymers: Poliamide-imide (PAI), Polyether-ether ketone (PEEK), Poly ether sulfone (PES), Poly-phenilensulfide (PPS), Polyeterimide (PEI): used as composite matrices with continuous fibers mainly graphite.
Technopolymers: Polyamides (6 o 6.6), thermoplastic polyesters (PET, PBT), Policarbonates (PC): largely used in injection molding with short reinforcing fibers. Also used with continuous fibers mainly glass
Commodity polymers: Polypropilene (PP) ): largely used in injection molding with short reinforcing fibers.

## Slide 6: Thermosetting polymer matrices
Epoxy: used mostly in aeronautical and aerospace applications.
Polyester and vinyl ester: used in automotive, marine, chemical and electrical applications.
Phenolic: used in bulk molding compound and used in internal components of public transport vehicles where the fire resistance is required.
Polyurethane: used when fast curing (1-3 min) is needed (automotive parts for example)
Polyimides, Bismaleimides (BMI), cyanate esters, polybenzimidazole (PBI), polyfenyl quinoxaline (PPQ): used in applications where high continuous use temperatures (250-300 °C) are required.

## Slide 7: Polymer matrices in aerospace

## Slide 8: Polymerization reactions
Linking of small molecules (monomers) to form macromolecules
Characteristics of polymerization reactions
Exothermic reactions (DTad=Dh/Cp)
Reactions accompanied by a reduction of volume (density increase)
Presence of at least two reactive groups per monomer
  There are secondary products, with some exceptions

## Slide 9: Heat of reaction
The crosslinking reaction is exothermic for all the resins used as matrices for composites.
For polyester and vinyl ester resins, the heat generated is proportional to the level of unsaturations of the chain and the amount of styrene.
The heat generated can further accelerate the curing of the resin. An excessive heat of reaction can lead to excessive shrinkage, cracking and degradation for thick layers of resin.

## Slide 10: Cure shrinkage for a vinylester resin
Cure
shrinkage

## Slide 11: Polymer Matrices
Bifunctional monomers Linear Polymers
Multifunctional monomers Crosslinked Polymers
Functionality of a monomer : number of links that a monomer can form

## Slide 12: Functionality of a monomer

## Slide 13: Curing Process
First molecular weight increases, then Gelation occurs.
Gelation: formation of an insoluble network
Vitrification: transition to the glassy state of the polymer (crosslinked or not) as a consequence of the increase of Tg with molecular weight or degree of crosslinking
Mw and
viscosity increase

## Slide 14: Curing steps
Flow(liquid- low viscosity)
  the matrix excess can be eliminated
  the trapped air is mobile and can reach the surface of the component
  Hydrostatic pressure in the resin prevent the porosity due to volatile compounds
  the distribution of the matrix becomes more uniform
  the matrix fills the gaps between the fibers (impregnation)
  the matrix act as adhesive between plies
Gel
  the material begins to harden due to crosslinking (mechanical behavior of a rubber)
  the viscosity becomes infinite
  the shape of the component can no longer be changed
Glassy solid
  - the material is now a rigid solid (elastic modulus of the order of 1 GPa)
  - the cross-linking is complete or almost complete
Notes: 14

## Slide 15: Gelation
Liquid
Gel: from solution to continuous network
Crosslinked
networks(microgels)
Catalysed
solution
GELATION: Covalent bonds start to connect the linear chains, forming regions of three-dimensional network.
The resin turns from liquid to rubbery.
The rate of reaction is not affected by
gelation
The viscosity dramatically increase,
Flow capability of resin are lost.

## Slide 16: Vitrification
Vitrification occurs when the glass transition temperature of the polymerizing resin exceeds the cure temperature of the resin.
The cure rate is significantly reduced, and further cross-linking occurs at a dramatically lower rate under the control of diffusion of molecules through the three-dimensional network.
The final physical state depends on the cure temperature.
Vitrification gives poor deformability and adequate stiffness to the material, so that it can be extracted from the molds.
In some cases, the resin can be further hardened with subsequent thermal treatments in oven called post-curing.

## Slide 17: Matrix: key parameters
Shelf life: time during which the matrix can be stored in specific environmental conditions (often at low temperature) retaining all the requirements of workability and performance
Pot life or Working life : time during which the properties of the matrix remain suitable for use after mixing all components (hardeners or catalysts or initiators). Resin flow with the required viscosity can occur before this time limit
Mechanical Life or Out Life: Fibers already impregnated by the resin are usually purchased: the so called prepregs. All resin components are pre-mixed and resins (prepregs) is stored at very low temperature (-20 °C). It is the time during which the properties of the matrix remain suitable for further processing.
Viscosity of the uncured resin: it decreases with temperature and increases as reaction progresses
Glass Transition Temperature (Tg): temperature above which the resin passes from a rigid glassy state to a semi-flexible material. A resin may never be used at temperatures above the Tg unless its service life is very short (eg. Nozzle of a rocket)
Cure time: for thermosetting resins is the time required for the polymerization reaction (curing) until the required Tg is achieved. In general, the high Tg resins have also longer cure times.
Notes: 17

## Slide 18: Glass Transition Temperature
GLASS TRANSITION TEMPERATURE (Tg): temperature at which a polymer, upon cooling, undergoes, the transformation from a rubbery state to a rigid state (the molecular mobility of 50-100 segments of the main chain is frozen).
The glass transition involves the amorphous phase of the polymer and is due to the reduction of mobility of macromolecular chains with decreasing temperature.
For T>Tg the polymer structure remains intact, but the crosslinks are no longer frozen in their positions: rotational mobility of molecules is allowed.
A thermosetting resin should never be used at T>Tg unless its service life is very short.
As a practical rule, the glass transition temperature Tg should be at least 50°C higher than the service temperature of the components. If the matrix absorbs easily moisture (and therefore its Tg decreases further) the Tg of the resin should be 100°C higher than the service temperature.

## Slide 19: The resin
Resin= Base monomer
Resin= Base monomer+ other monomers and or solvents
Resin= Base monomer+ other monomers and or solvents
+ Initiator or hardener
(curing agents)
The processability of a composite materials strongly depends on the following matrix properties:
Ø Viscosity
Ø Cure temperature and cure time
Ø Melting temperature (for thermoplastic matrices)

## Slide 20: Thermosetting matrices available on the market
Liquid monomers or oligomers +
Initiator or crosslinking agent (depending on the resin chemistry)
monomers
or oligomers
initiator or
crosslinking agent
Mix
Cure
Initiated
Room or
Hi Temp
reactive
Liquid
Crosslinked Solid

## Slide 21: Thermosetting matrices: resins
Liquid one-component
All components are premixed by the manufacturer. The cure is initiated by an increase in temperature or pressure or exposure to UV rays.
Cure Initiated
at high Temp.
Pre-mixed Liquid
with all reactive chemicals
Crosslinked Solid

## Slide 22: Thermosetting Matrices
Resin Type
Performance
Processing
Cost
LOW
HIGH
LOW
HIGH
DIFFICULT
EASY
Unsaturated Polyester
Polyurethane (PUR)
Vinyl Ester
Phenolic
Epoxy
Bismaleimide (BMI)
Polyimide (PI)
.

## Slide 23: Thermosetting matrices: property comparison
F.M. = Flexural modulus, F.S.= Flexural strength

## Slide 24: Thermoplastic matrices: property comparison

## Slide 25: Resin therma stability. Heat Deflection (Distortion) Temperature (HDT)
Riscaldamento uniforme
a 2°C/min
It is also called DTUL= Deflection Temperature Under Load
It is the temperature at which a given amount of deflection at a given applied load is reached.
It is lower than Tg for thermosetting and amorphous thermoplastic matrices.
Its between Tg and Tm for semicrystalline thermoplastic matrices

## Slide 26: Heat Deflection Temperature (HDT)
 | Tg °C | HDT=Max T operating °C
Thermosetting Matrices |  | 
DGEBA epoxy resin | 150 | 100
TGDDM epoxy resin | 200 – 220 | 150
Bismaleimide BMI | 230 – 290 | 232
Polymide ACTP | 320 | 280
Polymide PMR 15 | 340 | 300
Thermoplastic Matrices |  | 
Polyeter-eter-chetone PEEK (Semi-cryst.) | 143 | 180
Poly-phenylene sulfide PPS (Semi-cryst.) | 85 | 120
Polysulfone (amorphous) | 185 | 160
Polyetherimide (PEI) (amorphous) | 217 | 180
HDT is usually considered as the maximum operating temperature
It is lower than Tg for thermosetting and amorphous thermoplastic matrices.
Its between Tg and Tm for semicrystalline thermoplastic matrices

## Slide 27
Polymerization mechanisms
The final properties of a thermosetting matrix strongly depend on the conditions with which the monomers have been converted into the 3D network.
Chain polymerization
radicalic
ionic
Step polymerization
ring opening
polycondensation
Fast process, activated by an initiator, that proceeds by addition of a single monomer to a growing macromolecule (linear, branched or crosslinked).
Step process, reaction of functional goups of monomers and oligomers with formation of species with molecular weigth gradually increased.
Notes: 27

## Slide 28
CHAIN POLIMERIZATION
One or more monomers with only one reactive group
A reactive site is present at the end of the growing chain
^^^M* + M ^^^M-M*
Only the molecular species containing active centers can be added to the monomers.
Very fast chain growth: a polymer with high molecular weight quickly forms and the concentration of monomers decreases continuously during the reaction.
Monomer, polymer of high molecular weight and active centers are present at any reaction time.
STEP POLIMERIZATION
One or more monomers having at least two reactive group.
Any reactive molecular species can react and combine.
Initial formation of oligomeric products  rapid disappearance of the monomer immediately after the start of the reaction.
Reaction between oligomers with slow formation of polymeric products  slow increase of the molecular weight of the growing polymer.
Molecular species of any size are present at any reaction time.
Notes: 28