## Slide 1: Chemical bonds
H2 molecule. a) s type orbitals (separated), b) s type orbitals (superimposed), c) and d) bonding orbital s

## Slide 2: Methane
Elctronic configuration of C and H
1s 2s 2p
C CH2
H
Hybrid orbitals:
An electron is promoted from an orbital 2s to a 2p
4 hybrid orbitals sp3 are formed
4 unpaired electrons are now available to form 4 bonds
C CH4
4 s bonds of C with H, strongly directional, are formed

## Slide 3: Hybrid Orbitals sp3
Orbitals p and s
Atomic orbitals sp3. a) transversal section and approximated shape
b) simplified sketch of the orbital (the small lobe is omitted)
c) four orbitals with their axis oriented in the direction of tetrahedron axes.

## Slide 4: Bond angles of methane
Bonds in methane (CH4). a) Tetrahedral disposition of orbitals sp3 b) Position of H nuclei to obtain the maximum superposition of orbitals c) shape and size of bonds in methane

## Slide 5: Ethane
C
C
H
H
H
H
H
H
The C-C bond is also obtained from the overlap of orbitals sp3 with formation of a bond-type called “s”. The C-C and C-H bonds have cylindrical symmetry with respect to the line joining the nuclei. For them there is a fixed angle and bond distance.
Alcans CnH2n+2 T. eb.(°C)
Methane CH4 -162
Ethane CH3CH3 -88.5
Propane CH3CH2CH3 -42
-
-
n-Nonadecane CH3(CH2)17CH3 320
n- Eicosane CH3(CH2)18CH3 thermal decomposition

## Slide 6: Ethane stereochemistry
H
H
H
H
H
H
E, Kcal/mol
-60° 0° 60°
2.8
0
w
H
H
H
H
H
H
H
H
H
H
H
H
Eclipsed
Staggered
Staggered

## Slide 7: Butane stereochemistry (CH3CH2CH2CH3)

## Slide 9: Ethilene (CH2=CH2)
1s 2s 2p
C
Generation of hybrid orbitals.
An electron is promoted from a 2s to a 2p orbital
3 hybrid orbitals sp2 are formed (they result from the superposition of an orbital s and two p orbitals)
3 unpaired electrons form 3 s bonds: two of them
with the two H atoms and the other with C

## Slide 10: Ethylene
Atomic orbitals sp2. a) transversal section and approximated shape
b) simplified sketch of the orbital (the small lobe is omitted)
c) three orbitals with their axis oriented in the direction of tetrahedron axes.

## Slide 11: Ehtylene
Shape and size of ethylene molecule
Besides the three s bonds coming from the superposition of the hybrid orbitals sp2 there is still an electron available a p orbital in each carbon atom.
The superposition of these two p orbitals produces a new bond called p, characterized by two electron clouds above and below the s bond between the two carbon atoms
s E= 95 kcal/mole
p E= 48 kcal/mole
Ethylene molecule: Double bond C=C. Superposition of p orbitals generates the p bond with electrons above and below the plane of the molecule
Double (and triple) bonds are called unsaturated
No rotation is allowed when a C=C is present

## Slide 12: Ethylene

## Slide 13: Benzene C6H6
In every Carbon atom 3 sp2 orbitals over a total of 4 are used for s-type bonds.
C
C
C
C
C
C
H
H
H
H
H
H
120°
The p orbital, not hybridized, is orthogonal to the plane of sp2, (see ethylene) hence  to the molecule plane
Each p orbital is at the same distance from the other 2 non-hybridized of the adjacent C atoms: the probability of form a bond p with these adjacent atoms is the same.
The C6H6 molecule resonates between these two energetically equal forms:
p
s
p
s

## Slide 14: Some representative polymer functional groups

## Slide 15: Polymer: a possible definition
Organic compound deriving from the reaction of one or two types of small molecules called monomers (μόνος +μέρος). It is composed of a large number of molecules of the same type: polymers (polύs +μέρος).
The low molecular weight polymers, the smaller molecules, are called oligomers (όλιγος +μέρος) , polymers are also called mcromolecules
Many basic components of animals and vegetals are macromolecules, often much more complex than those synthesized
Their properties depends on the type of monomer, from the size of macromolecules, from their physical structure. Processing affects the physical structure development and in some cases also the chemical structure

## Slide 16: Bonding forces in polymer molecules
Intramolecular forces: primary bonds E= 50-200 kcal/mole
  covalent bonds (much less frequently ionic bonds)
Intermolecular forces: secondary bonds E= 0.5-10 kcal/mole
  Hydrogen, polar and Van der Waals bonds (in order of bonding energy)

## Slide 17: Factros affecting the intensity of bonding forces in macromolecules
Nature of secondary intermolecular bonding forces
Molecular architecture
  Molecular weight
  Steric hindrance
  Crosslinks
Distance among molecules
  Conformation
  Morphlogy and order (crystals) or disorder (amorphous)

## Slide 19: Looking inside linear polymers: thermoplastic

## Slide 20: Rotations around a s bond C-C can occur keeping fixed the bonding angle at 109°28’)

## Slide 24: Configuration and Conformation
Configuration
  Shape of a polymer chain resulting from the primary (covalent) bonds
Conformation
  Shape of a polymer chain resulting from the rotations around primary bonds
C
O
Rotational freedom decreases
(cfr. Rotational energy of buthane)

## Slide 25: Conformation of a polymer (i.e. polyethylene) corresponding to a disordered state (i.e. in the amorphous phase)

## Slide 26: Conformation of polyethylene corresponding to an ordered state (i.e. in a crystal)

## Slide 27: Polypropilene conformation in an ordered state (i.e. in a crystal)

## Slide 28: Crosslinked polymers are highly irregular and disordered: they are always amorphous

## Slide 29: Thermoplastic (linear) and thermosetting (crosslinked)
Thermoplastics: upon heating they melt and can flow filling molds.
  They can be melted many times and hence recycled
Thermosetting: upon heating they undergo a chemical reaction leading to a crosslinked structure that cannot melt.
  They cannot be melted upon heating and are very difficult to be recycled
  Adhesives composites Rubber

## Slide 30: Solubility parameter of a solvent
The solubility parameter is a measure of the intensity of the intermolecular secondary bonds
For a low molecular weight solvent:
Cohesive energy density (CED)=DEv/Vl e DEv=DHv-P(Vv-Vl)
DHv= molar heat of vaporization
P= vapor pressure
Vve Vl = molar volume of the vapor and liquid phase
Solubility parameter, d

## Slide 31: Solubility parameter of a solvent

## Slide 32: Solubility
Free energy of mixing:
    DFm=DHm-TDSm<0
  In ideal solutions DHm=0 and DSm>0 given by:
  DSm=-R[N1ln(1-x2)+N2ln(x2)]>0
  DFm=RT[N1ln(1-x2)+N2ln(x2)]<0 [eq.1]
  N1 and N2=moles of solvent and polymer
  x2= molar fraction of polymer
  In real solutions DHm is not 0 and [eq.1] does not hold anymore

## Slide 33: Solubility
To analyze the case in which DHm ≠ 0 Flory and introduced the interaction parameter c
    DFm= RT[N1ln(1-x2)+N2ln(x2)+ c (T)N2x2]
    DSm ideal solutions (always <0)
  c RT represents the interaction energy per mole of solvent for a given polymer-solvent pair
  c = cost+ (d1-d2)2 V1/RT
  d1,d2= solubility parametrs of the solvent and polymer
  V1=molar volume of the solvent
c <0.5 the polymer (amorphous and linear) is soluble
c =0.5 represents the limit of solubility and the temperature for which c =0.5 is called Flory q (theta) temperature and the solvent at this temperature is called a Flory q solvent

## Slide 34: Solubility parameter of a polymer
For polymers, the comparison is carried out using a weakly crosslinked polymer
To measure the solubility parameter of a polymer (dp), the polymer is put in contact with different solvents and its swelling is measured:
Q= (m-m0)/m0rs
  m anbd m0= swollen and initial weight of the polymer
  rs=Density of the solvent
Q
d
dp
Each point in the plot corresponds to a different solvent

## Slide 35: Solubility parameter of a polymer

## Slide 36: Solubility parameter of a polymer
Nylon 6

## Slide 37: Polarity of secondary bonds and surface energy
Solubility parameter or surface energy (a.u.)
PTFE
SILICONI
PP
PE
TPO
EPDM
SBR
PS
PVC
PMMA
Polyester
PC
epoxy
PU
PA
TPO Thermoplastic olefin
EPDM Ethilene-propylene-diene monomers
PC Polycarbonate
PU polyurethanes
PA polyamide
PMMA Poly-methyl-methacrylate
PTFE Poly-tertra-fluoro-ethylene
SBR Styrene butadiene rubber
PVC Poly-vinyl-Chloride
PS Poly-styrene

## Slide 38: Solubility parameter of a polymer
The solubility parameter is given by the contributions of different forces:
d2=d12+d22+d32=polar+H-bonding+ Van der Waals forces

## Slide 39
A solid state polymer can be:
Completely amorphous
Partially crystalline
- The amorphous fraction of a semicrystalline polymer can be glassy or liquid (polymer melt). In the latter case, it may have a liquid or rubbery behavior
Physic of polymers and transitions

## Slide 40: Physical states of a polymer: melted (or liquid)
In the liquid state (also called a polymer melt), the rotational mobility of at least 50-100 segments of the main chain around the bonds is allowed (within the limits of the restrictions imposed by bond angles, energy barriers etc.).
Molecules can easily slide over each other
Molecular mobility affects not only short-range vibrational or rotational motions but also long-chain rotational motions of the main chain

## Slide 41: Physical states of a polymer: “rubbery” state
It is the physical state of a crosslinked polymer melt
Also in this state, rotational mobility of the linear chain segments around the s bonds is allowed (within the limits of the restrictions imposed by bond angles, energy barriers, etc.).
The molecules can slide one over the other within the limits allowed by crosslinking
The term rubbery state is used, with some confusion, to indicate both a physical state and the mechanical properties of a polymer
A rubber is also a solid that exhibits very high non-linear elongations in the elastic field.
This behavior could be also find in non crosslinked polymers, as long as there are topological constraints to permanent molecular slipping (liquid like behavior)

## Slide 42: Physical states of a polymer: “glassy” state
Absence of rotations around the s bonds in the main chain.
At sufficiently low temperatures the rotation around the individual bonds becomes impossible due to the intra- and inter-molecular energy barriers
Even hydrogen atoms, linked to adjacent carbon atoms, can interfere with each other at sufficiently low temperatures (cfr. ethane energy barriers upon rotation)
Only vibrational mobility is allowed (at most also rotational mobility of very few chain segments and side groups)
Molecules get trapped in a completely disordered amorphous state
There are also physical constraints (entanglements) limiting long range molecular mobility

## Slide 43: Physical states of a polymer: “crystalline” state
Ordered structure, with long range order
The molecules are tightly packed so that intermolecular attraction forces stabilize the chains in a regular lattice.
This also happens if only Van der Waals inter-molecular forces are present

## Slide 44: Transition in polymers
Glass
Liquid
Glass transitions(Tg)
Crystal
Liquid
Melting (Tm)
Glass
Rubber
Glass transitions(Tg)
Crosslinked polymers
Linear or branched polymers
Crystallization (Tc)

## Slide 45
Tg (glass transition temperature) is the temperature below which the cooperative rotational mobility of 50-100 segments of the main chain ceases (intra- and inter-molecular energy barriers)

## Slide 46: 1) Glass transition as thermodynamic transition
1st order transitions:
  Discontinuity of v and h
Second order transitions
  Discontinuity of dv/dT (thermal expansion coefficient) Discontinuity of dh/dT (specific heat)
The glass transition can be considered a second order transition
Tg is obtained as limit value for experiments conducted by cooling at "infinitely" low speeds

## Slide 47: State diagram of an amorphous polymer
(Specific volume or enthalpy)

## Slide 48: State diagram of the crysatl phase of polymer: melting
Melting often involves a wide temperature range

## Slide 49
a fully crystalline polymer (not existing!)
D and F Elastic modulus 2-4 GPa
EElastic Modulus= 0.5-1.5 GPa
C (if crosslinked)=0.01-0.05 GPa

## Slide 51: Melting (Tm) and glass transition temperatures
The melting of a polymer occurs in a wide temperature range due to the different dimensions of the crystalline lamellae (due to different molecular weights, different length of regular sequences and above all to the formation temperature of the lamellae)
Tm >Tg always
For many omopolymers 0.5< Tg/Tm <0.7
 | Tg, °C | Tm°C | Tg/Tm[K/K]
PE | -125 | 135 | 0.5
PP | -18 | 176 | 0.57
PA6 | 47 | 225 | 0.64
Polyisoprene | -70 | 28 | 0.67