## Slide 1: CHAIN POLYMERIZATION
Only the molecular species containing active centers can be added to the monomers.
A polymer with high molecular weight quickly forms and the concentration of monomers decreases continuously during the reaction.
Monomer, polymer of high molecular weight and active centers are present at any reaction time.
STEP POLYMERIZATION
Any reactive molecular species can react and combine.
Rapid disappearance of the monomer immediately after the start of the reaction.
The molecular weight of the growing polymer increases slowly. The high molecular weight polymer appears at high degrees of conversion.
Molecular species of any size are present at any reaction time.

## Slide 2: Epoxy resins
Benefits:
Large variety of properties (toughness, flexibility, rigidity)
No emissions during curing
Low shrinkage during curing
Excellent resistance to chemical attack and solvents
Excellent adhesion to various materials
Excellent electrical insulating properties
Possibility of partial cure (oligomers)
Drawbacks:
Relatively high cost
Long curing reaction
Viscosity higher than polyester resins

## Slide 3: Epoxy resins

## Slide 4: Epoxy resins
Thermosetting matrices containing 2 or more epoxy rings, which are the reactive sites for the crosslinking reaction.
The simplest bifunctional epoxy resin belongs to the class of Diglycidylether of Bisphenol A (DGEBA).
DGEBA is very reactive through the epoxy groups with an active hydrogen-containing substances (alcohols, acids, amines).
H
H
Bisphenol A
DGEBA

## Slide 5: Epoxy resins- DGEBA
DGEBA epoxy resins can be characterized by higher molecular weight depending on the synthesis condition
Usually a resin contains molecules of different molecular weight, i.e n= 0, 1, 2 …..
These mixtures are chracterized by a fractional value of n. The low molecular weight resins are characterized by n=0.15. Resin that are solid at room temperature are charcaterized by n>2.5 up to n=18

## Slide 6: Epoxy resins- DGEBA

## Slide 7: Epoxy resins
Epoxy resins can be also characterized by aliphatic backbone, and leads to crosslinked polymers with much lower physical and mechanical properties, lower Tg but with high ductility

## Slide 8: Epoxy resins
Multifunctional epoxy resins: they have more than two epoxy rings and are used in high-performance composites.
Compared to bifunctional epoxy resins, they have:
higher cross-linking density
higher Tg and elastic modulus
higher chemical and thermal resistance

## Slide 9: Epoxy resins: curing agents (hardeners)
Crosslinking occurs primarily by step polymerization trhough curing agents containing 3 or 4 functional groups:
Primary or secondary amines
Anhydrides
Hydroxyls
Homopolymerization of the epoxy groups
Epoxy resins have a low shrinkage cross-linking because they do not give rise to reaction products during crosslinking.

## Slide 10: Curing agents: amines
Aliphatic amines: high reactivity and fast cure even at room temperature. They give to the matrix a good chemical resistance to solvents. The matrix cured with aliphatic amines can withstand up to about 100°C.
Cycloaliphatic amines : are very reactive at moderate temperatures and give good adhesion and excellent
chemical resistance.
Aromatic amines:
react at high temperature, giving the best mechanical performance to the epoxy matrices up to 150 °C. Used for the pre-preg.

## Slide 11: Curing agents: amines
The amines react with the epoxy groups through the hydrogens of the amino group.
Amine FUNCTIONALITY: number of hydrogen atoms of the -NH2 and NH groups.

## Slide 12: Epoxy resins: curing
The crosslinking reaction with amines occurs by reaction between the active hydrogen of the amine with the epoxy groups of the resin.

## Slide 13: Epoxy resins: curing
PRIMARY AMINE ADDITION: Opening of the epoxy ring and reaction with the hydrogen of the -NH2 amino groups.
SECONDARY AMINE ADDITION : The -NH amine group reacts with the epoxy ring of another molecule of DGEBA
Crosslinked polymer

## Slide 14: Epoxy resins: curing
PRIMARY AMINE ADDITION
SECONDARY AMINE ADDITION

## Slide 15: Epoxy resins: crosslinked structure
DDS
TGDDM
Amine reaction
Reaction with OH

## Slide 16: Epoxy resins: curing
REACTION WITH OH- OF EPOXY RESIN: the epoxy ring of a DGEBA molecule reacts with the hydroxyl of another DGEBA molecule, formed after the addition with a primary amine.
The reaction is favored only at high temperatures or T>120 ° C in the presence of Lewis acid catalysts (ad es. BF3 o BCl3)
CH2
CHOH

## Slide 17
Epoxy monomers

## Slide 18: Epoxy resins: curing
REACTION WITH ANHYDRIDES: anhydrides have a low reactivity with the epoxy so it is necessary to use accelerators (tertiary amines), high temperature treatment and post-treatment cycles.
Ring-opening of anhydride with a hydroxyl group to form an ester
Reaction of the carbossilic groups with epoxy
Other epoxy groups react with the already formed hydroxyl groups or existing hydroxyl groups

## Slide 19: Curing
Factors affecting the crosslinking density: - Chemistry (epoxy groups and their distribution) - Functionality of curing agents - Reaction conditions (time and temperature) - Chemical structure (epoxy groups and their distribution)
tensile modulus
glass transition temperature
thermal stability
chemical resistance
strain at break
fracture toughness
The increase of crosslinking density:
increases reduces

## Slide 20: Stoichiometric ratio epoxy-curing agent
Epoxide content (Epoxy Equivalent Weight EEW): weight in grams of resin containing 1 mole equivalent of epoxy (g/mol).
Mol Eq : mole equivalent of epoxy in 100 g
Amine hydrogen equivalent HEq (Hydrogen Equivalent Weight HEW):
grams of hardener containing one equivalent of N-H groups. It is obtained by dividing the molecular weight of the hardener by the number of active hydrogens per molecule of amine
Phr (parts per hundred resin): parts by weight of amine per 100 parts of epoxy resin

## Slide 21: Stoichiometric ratio epoxy-curing agent
Exampleo:
DGEBA: Mw=340 (g/mol) (g eq/mol)
TETA: Mw=146 (g/mol) (g eq/mol)
Epoxies are typically cured with stoichiometric or near-stoichiometric quantities of hardener to achieve the best physical and mechanical properties.

## Slide 22
The low reactivity can be improved adding a catalyzer such as a Lewis acid BF3MEA (monoethyl amine)
Aromatic amines for composite matrices

## Slide 23: Reactive diluents
Reactive diluents reduce the crosslinking density

## Slide 24: Epoxy equivalent of a mixture

## Slide 25: Properties of DGEBA base epoxy resins
DER 332 is an almost pure DGEBA resin and its viscosity is 4-6 Pas
DER 362 for example is obtained adding diluents possibly mono epoxide low viscosity compounds
DER 337 contains a solvent

## Slide 26
Epoxy resins: applications
http://www.bisphenol-a-europe.org
Epoxy resins constitute nearly 30% of total bisphenol A (BPA) use.