## Slide 1: Curing Process
Gelation: formation of an insoluble network
Vitrification: transition to the glassy state of the polymer (crosslinked or not) as a consequence of the increase of Tg with molecular weight or degree of crosslinking

## Slide 2: Cure Process
Chemical reaction
Heat evolution (heat of reaction)
Evolution of any volatiles
Increase in viscosity
Gelation--material won't flow
Vitrification--material hardens
Devitrification--degradation. (This is undesirable)

## Slide 3: Main process variables interacting among each other
Temperature
Degree of reaction
Viscosity

## Slide 4: Effect of Temperature
Cure kinetics
  Rate of reaction
  Maximum degree of reaction
Viscosity
Degradation of the resin

## Slide 5: Effect of the degree of reaction
Increase of molecular weight and viscosity growth (up to the gel point)
Degree of crosslinking and elastic modulus increase ( above the gel point)
Heat development
Environmental resistance

## Slide 6: Effect of viscosity
Fibre impregnation
Laminate consolidation
Resin flow
Pressure and energy for resin flow
Volatile (and air) expulsion

## Slide 7: The processing problem
Describe a complex process which involves heat, mass and momentum transfer with simultaneous chemical reaction in a multiphase system under conditions of time-dependent material properties and boundary conditions

## Slide 8: Process modeling
Transport phenomena
Energy
Mass (volatile diffusion)
Momentum (resin flow)
Composite properties
Thermal properties of composite and tools
Material behaviour
Cure kinetics
Rheology
(Crystallization kinetics in Themopl. Composites)
Geometry
Process design
Optimization
Production scheduling
Process Control
Residual stress and strains (distortions and spring in angle)
Process model
Initial and boundary conditions

## Slide 9: 1D Energy balance and kinetic model
Assumptions:
  Flat plane geometry
  r,Cp and k are constant
= heat rate generated by chemical reaction
= Dhref da/dt and da/dt = K(T) f(a)
a= degree of reaction or degree of cure. It can vary between 0 and 1
x
h

## Slide 10: Thermal properties of the composite
k1=vfkf+vrkr
1/k2=1/k3=vf/kf+vr/kr

## Slide 11: Energy balance : I.C. and B.C.
Initial conditions I.C.: t = 0 T = To e a = 0
Boundary conditions, B.C.:
  t >0 x = 0 T= T1(t)
  x = h T= T2(t)
  Convective boundary conditions and multilayer geometry can be easily included properly changing the former expression as will be explained later

## Slide 12: Dimensionless analysis
t*= t/tref x*= x/(h/2) q = (T-Tcure)/ DTref
DTref can be assumed as the maximum DT, generated by the reaction exotherm and allowable for the process (it changes depending on the quality of produced parts)
tref = tg = gel time calculated at aref = ag and T = Tref
Or
tref = t1/2 = time to reach a = 0.5 calculated at aref = 0.5 and T = Tref
tref is measured or calculated by integration of the kinetic model : da/dt = K(T)f(a)

## Slide 13: Dimensionless energy balance
Substituting the dimensionless variable ad dividing by r e Cp:
De= ktref/[rCp(h2/4)] St=Dhref/[CpDTref]

## Slide 14: Cure behaviour and dimensionless numbers
St = Stefan number =Dhref/[CpDTref]
The exothermic effects associated with the heat produced by the reaction are relevant in relation to the assumed al DTref (the allowable limit) if:
St O(1) Or St >1

## Slide 15: Cure behaviour and dimensionless numbers
De = Diffusive Deborah Number
Deborah number was first defined as the ratio of a relaxation time to the time scale of the experiment from Judges 5:2-31, the song of Deborah: “The mountains flowed before the Lord”

## Slide 16: Cure behaviour and dimensionless numbers
If St is of the order of 1 or higher than 1 then exothermal effect could be relevant and the value of Deborah number indicates:
  De<<1 Adiabatic behaviour
    td >>tref Tmax=Tcure+Dhref/Cp
  De >>1  Isothermal behaviour
    td <<tref
  De O(1)  The temperature rise into the composite must be calculated solving the energy balance coupled with the cure kinetic equation.

## Slide 17: Glass transition evolution during curing
Tc
-50
0
50
100
150
200
Tg
Cure temperature
Time
Tgo

## Slide 18
Tc
-50
0
50
100
150
200
Tg
Glass transition evolution during curing
Cure temperature
Time
Tgo

## Slide 19: Glass transition evolution during curing
Tc
-50
0
50
100
150
200
Tg
Cure temperature
Time
Tgo

## Slide 20: Glass transition evolution during curing
Tc
-50
0
50
100
150
200
Tg
Time
Cure temperature
vitrification
Tgo

## Slide 21
Tc
The Tg of the resin will be only slightly higher than Tc
Step polymerization (epoxy resin) Tg=Tc + (5¸10) °C
Chain polymerization Tg=Tc + (10¸20) °C
-50
0
50
100
150
200
Tg
Glass transition evolution during curing
Time
Cure temperature
Tgo

## Slide 22: Curing Process: TTT Diagram (Time-Temperature-Transformation)
Acceptable Temp. interval for curing

## Slide 23: Curing Process: TTT Diagram
Between Tg0 and TgGEL, the catalysed solution is in a liquid state. Crosslinking occurs until vitrification, where a transition to a glassy solid is made, BUT gelation does not occur !
The reaction is very slow thereafter.
Below Tg0 the catalysed solution will be a glassy solid. The crosslinking reaction can only occur very slowly, by diffusion (months or years). Thermosets used in prepregs are stored below Tg0 to allow storage time of about 1 year

## Slide 24: Curing Process: TTT Diagram
Above Tg¥: the catalysed solution is in a liquid state. Curing is very fast and vitrification never occurs. Higher temperature could be reached due to the exothermic heat of reaction delivered in a very short time. Degradation could also occur if temperature is too high or if the composite is held at high temperature for a too long time.
Between TgGEL and Tg¥: the catalysed solution is liquid. In this temperature range the cure reaction must occur, leading to a crosslinked resin. After vitrification the reaction becomes diffusion controlled, becomes very slow and the process is stopped beginning the cooling stage

## Slide 25: Cure Process: plot of h (or v) vs. T at different a
a = 0
a = 1
T
h (or v)
Tg¥
Tc
Tg0
rubbery state
TC is too low and the resin can become a glass but not a gel
Gelled glassy state
a = ag
Dh (Dv)
gelTg
liquid state
Ungelled glassy state

## Slide 26: Calorimetric analysis to study cure kinetic
dh/dt
h (t)

## Slide 27: Calorimetric analysis
Degree of reaction
Dhref= reference heat of reaction (or maximum heat of reaction)
BL= Baseline
P=Sample mass
Dhiso

## Slide 28
Dhiso < Dhmax
Dhmax

## Slide 29: Experimental DSC analysis of an epoxy resin
Isothermal DSC: maximum
degree of reaction amax<1
Dynamic DSC: maximum
degree of reaction amax=1

## Slide 30: Dependence from temperature of isothermal heat of reaction
Dhis
Dhmax
Tc¥ Tg¥ cure temperature
Chain polymerization Dhmax Tc¥ =Tg¥ – (10¸30) °C
Step polymerization Dhmax Tc¥ =Tg¥ – (5¸10) °C

## Slide 31: Relationship between Tg and a
Di Benedetto equation
a = 0Tg = Tgo and a =1Tg = Tg¥
C1/C2 = Tg¥/Tgo
        Tg¥
        Tgo
0 1
Degree of reaction

## Slide 32: Relationship between a and Tc: definition of amax
        amax
        cure temperature Tc¥
Di Benedetto eq. can be inverted and Tc substituted to Tg. amax is then expressed as a function of Tc :
More often a linear dependence of amax from Tc is assumed, when amax is close to 1:
amax = a +b Tc for 0.6 < amax < 1
amax = 1 for T > Tc¥
0
1

## Slide 33: Which data I can collect from DSC analysis
Basic information:
dynamic scans on prepregs and cured samples lead to Tgo, and Tgmax
dynamic scans run above Tgmax , allow to measure Dhmax.
Tg(Tcure) is obtained by a dynamic scan after an isothermal test performed below Tgmax
Isothemal DSC tests allow to measure the heat of reaction corresponding at each curing temperature ,Dhiso, and amax
Higher level information:
The shape of a DSC test in isothermal conditions is proportional to the function representing the rate of reaction da/dt that is obtained after subtraction of baseline and normalization by sample weight and Dhmax.
Integration (numerical) of DSC measured heat flow, normalized by sample weight and Dhmax or direct integration (numerical) of da/dt allows to obtain the degree of reaction a(t)

## Slide 34: Glossary
dH/dt and dh/dt: heat flow (mw) and heat flow normalized by sample weight (W/g) respectively as measured by DSC
BL: Baseline used for integration of DSC thermograms
Tgo : the glass transition of an uncured resin
Tgmax or Tg∞: maximum glass transition temperature of a resin
Tc∞:the minimum curing temperature allowing to reach the maximum glass transition temperature of a resin. Usually, some °C lower than Tgmax = Tg∞
Dhmax : Maximum heat of reaction used as reference value in normalization of DSC results
Dhiso : isothermal heat of reaction, always< Dhmax
amax: maximum degree of reaction obtained as the ratio between Dhiso and Dhmax . It is reached at the end of an isothermal curing process below Tc∞ .
da/dt: rate of reaction (a function of time and temperature) obtained by isothermal and dynamic DSC scans
a(t,T): degree of reaction obtained by integration of da/dt

## Slide 35: CHAIN POLYMERIZATION
Only the molecular species containing active centers can be added to the monomers.
A polymer with high molecular weight quickly forms and the concentration of monomers decreases continuously during the reaction.
Monomer, polymer of high molecular weight and active centers are present at any reaction time.
STEP POLYMERIZATION
Any reactive molecular species can react and combine.
Rapid disappearance of the monomer immediately after the start of the reaction.
The molecular weight of the growing polymer increases slowly. The high molecular weight polymer appears at high degrees of conversion.
Molecular species of any size are present at any reaction time.
ag < 0.1
0.3<ag <0.6

## Slide 36
Step polymerization: statistic approach
Given two monomers ARA and BR’B with A and B two reactive functional groups
FA= Number of A functional groups
PA=[FA(0)- FA(t)]/ FA(0) 0< PA<1
If A and B are in stoichiometric balance: PA=PB=P
If A and B are not in stoichiometric balance
PA¹PB  PB/PA=FA(0)/FB(0)=r
As a consequence of: FA(0)- FA(t)=FB(0)- FB(t)

## Slide 37
Degree of polymerization :
Xn=[Mo-M(t)]/P(t)
Xn=N°of initial monomers-N° of monomers at time t
N° polymer molecules
Mn=SiNiMi = Total polym. weight= MmMo = MmMo= XnMm
SiNi N° of molecules SiNi P(t)
Assuming that M(t)<<Mo and negligible as soon as the reaction begins.
Mm represents the molecular weight of the monomers (in absence of any secondary products)
Xn is a measure of the average molecular weight
Step polymerization: Degree of polymerization

## Slide 38: Step polymerization: stoichiometry and degree of polymerization
Hypotesis:
  ARA and BR’B
  r=FA(0)/FB(0)<1 (excess of B)
Total number of monomers at t=0 Mo:
Mo= [FA(0)+FB(0)]/2 = [FA(0)(1+1/r)]/2 (eq.1)
The polymers at any time t can be of the following types
A------B B------B A------A
Since B is in excess, the last polymer should never be present (low probability to occur)
The number of polymer chains is obtained counting the number of chain ends and then dividing by 2

## Slide 39: Step polymerization: stoichiometry and degree of polymerization
The number of chain ends associated with the molecules A----B
2FA(0)(1-PA) (stoichiometric ratio)
The number of chain ends associated with the molecules B----B
FB(0)-FA(0) (depending from the excess of B)
Number of molecules of polymer P(t)
Eq(2)

## Slide 40: Step polymerization: stoichiometry and degree of polymerization
If M(t)<<Mo then, the degree of polymerization is:
Xn= (Mo-M(t))/P(t) @Mo/P(t)
substituting Eq. 1 and 2:

## Slide 41: Step polymerization: stoichiometry and degree of polymerization
In the special case r=1Xn=1/(1-P) (PA=PB=P)
In order to reach a high molecular weight P>0.99!
2) In presence of a small excess of B, for instance:
r=100/101if PA=1 Xn=201
P | 0 | 0.5 | 0.8 | 0.9 | 0.95 | 0.99 | 0.999 | 1
Xn | 1 | 2 | 5 | 10 | 20 | 100 | 1000 | ¥

## Slide 42
When one of the reactive groups is in excess an effect called “blocking” occurs  it is mandatory to keep the stoichiometry ratio in order to get high molecular weights
On the other hand, the blocking effect can be used to produce oligomers. This effect is exploited for the synthesis of novolacs and for the synthesis of unsaturated polyester oligomers
When dealing with thermosetting resins, changes (errors!) of stoichiometry are responsible of less drastic effects. Usually, Tg can change depending on the type of monomer in excess. For instance, in the case of a resin made of an epoxy monomer with f=2 and an amine with f>4:
  an excess of epoxides determines a strong reduction of Tg due to the formation of “dangling ends”, connected only on one side to the network
  an excess of amine produces lower effects on Tg (the formation of a crosslinking point needs the reaction of just three hydrogen atoms over 4)
  In both cases unreacted -NH or epoxides are strongly hydrophilic and the amount water that can be absorbed is higher.
Step polymerization: stoichiometry and degree of polymerization

## Slide 43: Stoichiometry and Tg
In the case of DGEBA (f=2) and TETA (f=6) the stoichiometric ratio corresponds to14 PHR.
An excess of amine determines limited changes of Tg:
  The reactivity of 3 to 5 hydrogens (less than 6) is still adequate to determine crosslinking without dramatic changes in the network
An excess of epoxy monomers determines significant changes of Tg :
  An unreacted epoxy group on a monomer with f=2 produces a dangling end connected only on one side to the network
Phr | Q (J/g) | Tg (°C)
12 | 406 | 90
14 | 498 | 127
16 | 490 | 125
18 | 480 | 124
Excess of epoxide
Excess of amine

## Slide 44: Dangling ends
Dangling end
C----C
O
= crosslinking point on an amine f=4 and 4 reacted H
= crosslinking point on an amine f=4 but 3 reacted H

## Slide 45: Radical chain polymerization: kinetics
Initiation
A= Active species, M=monomers
2. Propagation
. . .
. . .

## Slide 46: Radical chain polymerization: kinetics
3. Chain transfer (not relevant for thermosettings)
Pm or Pn = “dead” polymer, P-H chain transfer agent, P·=radical on the side of the chain P
4. Termination
Recombination
(the most relevant)
b) Disproportionation (negligible)
Pmu= polymer with unsaturated bond

## Slide 47: Radical chain polymerization: kinetics
Hypotesis
  Constant concentration of the active species  Vi=Vt ( “steady state” hypothesis)
  Same reactivity of active species An independently from the Mw (or length) of the molecules at which they belong
Initiation (Vi)
Integrating adopting as I.C.:t=0 [I]=[I0]

## Slide 48: Radical chain polymerization: kinetics
2. Propagation (Vp)
chain transfer
3. Termination (Vt)
(Hypothesis of same reactivity)

## Slide 49: Radical chain polymerization: kinetics
Introducing the hypothesis of steady state : Vi=Vt
Substituting in the expression for propagation kinetic

## Slide 50: Radical chain polymerization: kinetics
The rate of reaction can be expressed as the time derivative of:
degree of reaction
a=([Mo]-[M])/[Mo] called degree of cure (thermosetting resins)
conversion
However this expression fits experimental data for a<0.2 (about)!

## Slide 51: Radical chain polymerization: Autoacceleration or (Gel effect) or Trommsdorf effect
Neglecting the changes of [I] in the kinetic of propagation in steady state:
Integrating by separation
of variables:
ln (1-a) = -kt
an hence a=1-exp(-Kt)
MMA T=0°C with a photo-initiator (X=a)
[I0]

## Slide 52
Termination occurs in three steps:
Translational diffusion: two radicals, linked to different macromolecules (coils), get close, i.e. at a distance comparable with the size of the coil. (kinetic constant kd)
Radical chain polymerization: Autoacceleration or (Gel effect) or Trommsdorf effect

## Slide 53
2. Segmental diffusion: conformational rearrangements of the two coils lead the radical enough close to allow the termination reaction (kinetic constant ks)
Radical chain polymerization: Autoacceleration or (Gel effect) or Trommsdorf effect

## Slide 54
3. Chemical step of the termination reaction: the two radicals combine to give rise to a dead polymer P.
Obviously, the reaction can also occur with initiator radicals or with radicals linked to very small molecules (for instance if you have used an excessive amount of initiator ) The overall constant termination kt is therefore dominated by the slower process (the smallest of the three among ks, kd e kR). The diffusion processes mainly affect termination when the mobility of radicals bound to macromolecules drops the rate of termination drops and an increase in radical concentration is observed.
Radical chain polymerization: Autoacceleration or (Gel effect) or Trommsdorf effect

## Slide 55
Re-arranging the expression obtained in steady state for the rate of propagation:
= constant (T=const.)
IA. Propagation rate divided by [M] and [I]0.5 is constant (according to steady state hypothesis)
II. Autoacceleration
IIIB. Further diffusive effects that determines a reduction of Rp (vitrification as discussed later)
Rp=-d[M]/dt
a=0.2 about
Radical chain polymerization: Autoacceleration or (Gel effect) or Trommsdorf effect

## Slide 56: Autoacceleration
Effect of the addition of a non-reactive solvent (benzene) to the monomer (MMA).
It is a solvent of both monomer and polymer
a=0.2 circa
Autoacceleration moves at longer times and higher degree of reaction for more diluted solutions

## Slide 57: Autoacceleration
Effect of the addition of PMMA to MMA in presence of 2 Phr of benzoyl peroxide initiator (Bz2O2)
With the increase of the amount of PMMA the value of the degree of reaction corresponding to the onset of autoacceleration (C¯) is anticipated
a=c/100
=1-a

## Slide 58: Autoacceleration
a=c/100
Effect of the addition of PMMA to MMA: time to reach the onset of autoacceleration, corresponding to (C¯) in the former figure

## Slide 59: Total hip prosthesis
Cemented Not Cemented
https://www.youtube.com/watch?v=7BCPpMHbfIQ

## Slide 60: Autoacceleration: thermosetting polyesters and vinylesters
The autoacceleration occurs when the mobility of radicals bound to large molecules becomes very low.
Gelation occurs to a degree of reaction at the most equal to 0.1 in radical chain polymerization among monomers with f> 2.
For radicals linked to a gel, translational mobility is impossible (KD=0) and the rotational mobility is strongly reduced
Therefore, at gelation, or even before, autoacceleration occurs (Kt very small).
The final effect is that as soon as the propagation reaction starts, after the induction time is consumed, autoacceleration occurs

## Slide 61: Kinetic models
t
t
#1 adopted for epoxy resins
#2 adopted for polyester and vynil ester resins
(pseudo- autocatalitic)
ti=Induction time
ti

## Slide 62: Kinetic models
t
The effect of vitrification lead to stop the reaction for a<1
m and n are pseudo reaction orders.
The model #1 per K2=0 ed il #2 per K1=0 are obtained
K1 e K2 depend from temperature according to an Arrhenius expression
and

## Slide 63: Chain cure reactions: dynamic DSC scan on a vynilester resin
the heat flow is constant in the highlighted Temp.interval

## Slide 64: Chain cure reactions: dynamic DSC scan on a vynilester resin
the heat flow is constant in the highlighted Temp.interval

## Slide 65: Chain cure reactions: dynamic DSC scan on a vynilester resin
Kinetic model
The plateau is due to vitrification occurring during heating. The rate at which Tg increases is higher than the rate at which T grows in the DSC
On further heating the temperature becomes higher than the Tg and the reaction re-start assuming a (almost) constant rate, proportional to the heating rate of the sample in the DSC.

## Slide 66: Radical chain polymerization: induction time
Inhibition reaction (inhibitor = Z reacts with radicals at higher rates than monomers: a radical scavenger)
f[Zo]=2e([I0]-[Iz])
con 0<e<1= efficiency of initiator
0<f<1=efficiency of inhibitor
[Iz]= Initiator concentration when all the inhibitor is consumed at [I]=[Iz] propagation starts
Therefore [I]=[Iz] when t=ti= Induction time (or working time)

## Slide 67: Radical chain polymerization: Induction time
f[Zo]=2e[I0][1-exp(-kiti)] with ki=koiexp (-Ei/RT)
Induction time ti, is obtained from the former equations as a function of the temperature once initial concentrations of inhibitor [Zo] and Initiator [Io] are fixed:
ti, can be obtained as a function of the temperature from an inverse Arrhenius like expression
ti represents the “working” time, i.e. the time during which viscosity remains constant before reaction starts and viscosity rapidly increases up to gelation

## Slide 68: Induction time in radical cure reaction and initial conditions
In this case the initial condition to be adopted for the kinetic model is :
t = ti a = 0; ti induction time = K exp (-Ei/RT)
In non isothermal conditions, i.e. N discrete steps at Tk:
Dt1 Dt2 Dtk t
T
Tk
T2
T1
Per Ninfinite and Dtk0
a = 0 until f < 1

## Slide 69: Convective boundary conditions (open mold processes: autoclave lamination, filament winding, hand lay up)
T at x = 0 at the composite-air interface is now not fixed and must be determined form the solution of energy balance with this B.C.
The dimensionless B.C. is:
Bi<<1 the interface behaves as adiabatic
Bi >>1 the interface temeperature is close to environment temp., To (isothermal behaviour)

## Slide 70: Continuity conditions at the boundary between two materials (interboundary conditions) (sandwich panels, and any composite process modeling the laminate together with the mold)
At the interface, temeprature and heat flow must be continuous
T2,A=T2,B…..Ti,N=Ti,N+1
-kA (¶TA/¶xA)2 = -kB(¶TB/¶xB)2……. -kN (¶TN/¶xN)i = -kN+1(¶TN+1/¶xN+1)i
The dimensionless form is:
(¶q/¶xA*)2=[(kBhA)/(kAhB)] (¶q/¶xB*)2 x*A=xA/hA x*B= xB/hB
1 A 2 B 3 C 4 …… N i N+1
hA hB hC hN hN+1

## Slide 71
Resin viscosity
The function f(T) can be :
a WLF expression or an exponential
In WLF eq. Tg changes as a function of a should be considered:
Also Di Benedetto eq. can be adopted
ag= degree of reaction at gelation A, B= Constants not dependent on temperature
Viscosity of the resin is a function of temperature and degree of reaction

## Slide 72
(Kenny et. al. 1990)
(Maffezzoli et. al. 1994)
Epoxy resin
TGDDM-DDS

## Slide 73: Modeling results: sudden heating at cure temperature
Thickness 14 mm
Tcure = 177 °C
q= Temp. Adimensionale
h/hr
ag

## Slide 74: Numerical solutions of energy balance and kinetic equation: Temperature at skin and core of the composite laminate
Mid plane temperature
Temperature, °C
Time, s
Imposed temperature at B.C.

## Slide 75
Numerical solutions of energy balance and kinetic equation: degree of reaction at skin and core of the composite laminate
degree of reaction at mid plane
Time, s
Degree of reaction at the skin
where B.C. are imposed
ag

## Slide 76
Numerical solutions of energy balance and kinetic equation: degree of reaction at skin and core of the composite laminate
Viscosity at mid plane
Time, s
Viscosity at the skin
where B.C. are imposed
Ln viscosity, Pas

## Slide 77: Crritical parameter in autoclave lamination
Choice of auxiliary materials
Resin content and resin hydrostatic pressure
Void (porosity) removal
Vacuum and pressure on the laminate (and cores)
Thermal history