## Slide 1: Filament winding

## Slide 2: Filament winding equipment

## Slide 3: Filament winding of prepregs
Uses a continuous length of fiber strand, roving, or tape
Results in a shell of materials with a high strength-to-weight ratio
Requires thermal curing of workpieces
Patterns may be longitudinal, circumferential or helical.

## Slide 4: Filament winding equipment

## Slide 5: fiber placement or filament winding ?

## Slide 6: Defects in fiber placement multi-tow

## Slide 7: Filament winding: fiber impregnation

## Slide 8: Filament winding: fiber impregnation

## Slide 9: Filament winding: fiber feeding
Comb
Important parameters:
control of the resin temperature (to have optimal viscosity level) .
fiber tension(also promotes air expulsion from the roving) often not controlled with a load cell but depending on solid and viscous friction
determines the bandwidth. It depends on the fiber diameter

## Slide 10
Fiber tension
TENSION MECHANISMS
Tension mechanisms must avoid stresses that could damage the fibers.
1° level tension: Solid-solid friction by a system of ceramics guides
Filament winding: fiber tension

## Slide 11
Filament winding: fiber tension
TENSION
2° level tension: Adjustable steel bars with different angles depending on the applied tension.
Tension increase
3° level tension: the bobin is equpped with a torque meter that can be set to a given value

## Slide 15: Filament Winding: winding patterns
(not common)

## Slide 16: Filament Winding: winding parameters
 winding angle
vp mandrel speed
vt translation speed of the deposition comb
h bundle bandwidth
p winding pitch
n numbers of runs

## Slide 17: Helical windings on cylindrical surfaces
The winding angle (q) is defined by the ratio between the mandrel peripheral speed (vp) and the speed of translation of the deposition comb (vt).
q is defined from design. q determines the ratio between the two speeds
tanq=vp/vt= w (D/2+s) /vt = p (rpm/60) (D/2+s) /vt
rpm=round per minutes of the mandrel
w=angular velocity
s= thickness.
Thickness progressively increases at every run of the comb. To keep q constant, the ratio rpm/vt (or w/vt) is usually adjusted increasing vt at each run of the deposition comb.
vp=wD/2
vt
q
D

## Slide 18: Helical windings on cylindrical surfaces
n=1
p
h
z
development of the mandrel in the plane
in the general case more deposition runs of the comb are necessary to complete a coating
each coating may be represented by an antisymmetric laminate with fibers[+q]
n=2
pD

## Slide 19: Helical windings on cylindrical surfaces
The deposition parameters are:
  h: the width of wound fiber bundle (even more than several cm if several spools and a comb are used)
  n: number of runs along z to make a complete covering
The pitch p is defined as the distance along z between two bundles.
If the deposition occurs at a constant speed along z, then the pitch must be an integer multiple of the bandwidth:
n=1
p
h
z
development of the mandrel in the plane

## Slide 20: Helical windings on cylindrical surfaces
In the extreme case of a full covering in just one run (n = 1), then p=hmax
in this case pD/hmax=pD/p=tgq.
Once obtained p, the actual width h will have to be a sub integer multiple of
p: h=p/n.
E.g. for D=400 mm and q=55° p=hmax=1800 mm
If I want to complete a covering with n=6, then h=1800/6=300 mm= bundle width to be used during covering
Conversely, if the comb allows to wind a bundle width h=100 mm n=1800/100=18
n=1
p=hmax
z
pD
q
q
development of the mandrel in the plane

## Slide 21: Standard pipes: fiber angle
T= resultant force in the a direction (the winding angle), must be determined
sq= circumferential stress= PR/s (Mariotte equation)
sx= axial stress that, for a closed pipe, is obtained from the equilibrium of forces in the x direction PpR2=2pRssx from which sx=PR/2s
Equilibrium of forces on a small surface element of the cylinder with thickness s.
sq= PR/s=T sena /(dx s)
sx= PR/2s=T cosa /(dx s tana)
By dividing member to member one can get
Which corresponds to an angle a of 55°
For a pressure P the resultant of the forces is at 55°standard winding angle
a
s
dx
dx tana
T
sx
sq

## Slide 22: Filament Winding: movies
https://www.youtube.com/watch?v=ign6W5ENJAA
https://www.youtube.com/watch?v=4ihtyjydzqA
https://www.youtube.com/watch?v=DAdmo8ZCNfU
Continuous process
https://www.youtube.com/watch?v=uePn-UP0xc4
https://www.youtube.com/watch?v=yDFrWFi64ew
https://www.youtube.com/watch?v=14bVB5KYBsI

## Slide 23: Filament Winding
Materials
  carbon, glass and aramide fibers
  epoxy, polyester, vinylester and phenolic matrices
Process characteristics
  Impregnation during the process (wet FW) or more rarely with prepregs (dry FW)
  Winding angles >10° and <85°
  At least 2 degrees of freedom (mandrel rotation and comb translation). Machines up to 6 degrees of freedom  similar to ATL or AFP.
  Helical winding:  angles>20°. The fiber bundles are not wound adjacent to one another. The winding pitch is higher than the bandwidth. Each covering is simulated as two laminae oriented at + . Hoop winding is performed at  close to 90°.
  Polar or Planar Winding:  angles<20°. Typical winding used for tanks or structures subjected to bending. Longitudinal winding can be performed only using prepregs and AFP machines
  Geodesic fiber path: the fiber is wound on the shortest distance between two points.
  Bridging can occur on concave surfaces, also mandrels with flat surfaces are not suitableOnly convex surfaces can be wound.
  Winding speed variable, up to 150 m/min.

## Slide 24: Mandrel materials
Mandrel characteristics
  They must withstand the compression forces caused by the fibers during winding and have a high axial stiffness (eg. for pipes)
  They must retain sufficient mechanical properties at high temperature
  They must be easily removed and withstand to the forces applied for extraction
Materials used for mandrels
  Not collapsible mandrels
  generally of steel and used for geometries that allow for their extraction ("draft angle")
  Collapsible mandrels : removable in metal or more rarely in composite
    Inflatable rubber mandrels
    Water soluble (for example mixtures of sand and PVA)
Fiber tension is associated to component normal to the mandrel surface which determines a pression P on the mandrel. The reinforcement “move” toward the mandrel axis in presence of a viscous resistance to the radial motion of the fibers will balance according to the Darcy eq:
Q/A=-(K/h) (DP/l)
A higher fiber content is found close to mandrel surface and a higher resin content on the external side

## Slide 25: Collapsible mandrels
Experiments on a fuselage of a business jet
  composite skin
  4 parts of which 2 are removed and 2 others retracted towards the center

## Slide 26: Typical pipe configuration
Pipes are made by a minimum of 2layers up to to 4 layers. From the inside:
Liner chemical resistant such as:
  Thermoplastic polymers (PVC and HDPE but also fluoropolymers)
  Composite with C-glass fiber content < 20% or with PET veils
  Metallic (especially for pressurized gas)
Fiber reinforced mechanical resistant layer
Wear and impact resistant layer
Thermal insulating layer
Example of a spoolable pipe for
oil and gas
1
2
3
4

## Slide 27: Filament wound pipes

## Slide 28: Pressure vessels (CNG=Compressed Natural Gas)

## Slide 29: Pressure vessels (CNG=Compressed Natural Gas)
Minimum Burst ratio= Safety factor
Cylinder means here a pressure vessel
Type 5: full composite pressure vessels

## Slide 30: Cost breakout of a 700 bar H2 pressure vessel

## Slide 31: BMW solution: cryo-compressed tank
-40 °C: cooling required before refuelling at 700 bar to limit max temp. < 85°C
Cryo-compressed (CcH2) at 350 bar and 80 k 63kg/m3

## Slide 32: Impact on carbon fiber market
Tons of Carbon fibers
The graph shows projected carbon fiber usage (metric tons) in Type IV 700-bar compressed H2 gas tanks for the highest production volume fuel cell vehicles (FCV). The table shows that these 2030 projections are conservative, for example, less than 1% of current car production will be FCV in 2030.
In 2020 CF production is estimated in 130 ktons
Composites world Oct. 2021

## Slide 33: Applications: rail and buses
Alstom has sold 41 Coradia iLint H2 trains to Germany
With a 1,000-kilometer range and a top speed of 140 km/hour, it matches current regional train performance. Its two-car units use 24 Type IV tanks housed in a rooftop compartment atop each car, which also contains
the fuel cells.
Composites world Oct. 2021

## Slide 34: Complex shapes

## Slide 35: High performance composites

## Slide 36: Filament winding: critical parameters
Resin viscosity for wet FW (tipically 0.3-1.5 Pa*s)
Pot life
Fiber tension (slippage, radial movement and bridging)
Resin content and distribution
Adhesion among different layers (e.g. between liner and mechanical resistant layer)
Curing conditions
  Room temperature and eventual post-curing
  IR lamps and eventual post-curing
  Oven
  Autoclave with vacuum bag
  UV lamps

## Slide 37: Filament winding: process modeling
Submodels
  Fiber location (layer alternation of layers and pattern design, thickness of layers, fiber content, final thickness)
  Energy balance in the mandrel (H= 0) and in the composite:
  Kinetic: da/dt=K(T)f(a)
  Rheological: h=h(T,a)
  Stress state caused by the tension of the fibers and by the curing effects and temperature